CONSTRUCT 09/880

QUERIES - CONSOLIDATED SITUATION 25-01-2010

QUERIES CONCERNING ALREADY CITED hENs

| EN TITLE | COMMENTS | CEN POSITION | WAY FORWARD |
| --- | --- | --- | --- |
| EN 845-1:2003+ A1:2008: Ties, tension straps, hangers and brackets standard | FI Comments: Standard included some serious deficiencies from the point of view of a regulator. The deficiencies are the following: - Clause 5.3: Characteristic load bearing capacity shall be given for those ancillary components (i.e. tension straps, hangers and brackets) which are acting independently. For example timber beam is designed based on characteristic load bearing capacity. That is why the bracket supporting the beam should also be designed based on characteristic load bearing capacity, not based on mean load bearing capacity. - Clause 5.3.4: The standard EN 845-1 is based only on testing. However load bearing capacity of slip ties (head restraint type) is declared based on calculation according “accepted engineering principles”. This not acceptable and these ties should be removed from the standard or test methods should be developed. - Clause 8.3: More precise FPC rules are needed. For example testing frequencies for FPC characteristics shall be specified. There is no notified body position paper concerning these products. - Table ZA.1: All the information given in the table 1 is related with the mandated characteristics. This shall be given in table ZA.1 as proxy characteristics. - Figure ZA.1: CE-marking example needs complete rewriting Note: Standard EN 845-1 is under review in CEN TC 125. New EN 845-1 will include improvements compared to the existing EN 845-1:2003 but it seems that the deficiencies presented above will not be solved. |  |  |
| EN 845-2:2003 Lintels | FI Comments: Standard includes a lot of serious deficiencies from the point of view of a regulator. The main deficiencies are the following: - General: The mandate M116 and table ZA.1 in the standard specify the lintels to support the loads over openings in masonry walls with a semi-structural role in the works. It is not specified what the semi-structural role actually means. In any case in Finland lintels are also used to support the loads over openings in masonry walls with a (normal) structural role in the works. Proposal: The mandate M116 shall be modified to cover lintels with a (normal) structural role in the works and a harmonised product standard shall be prepared for them. Scope of EN 845-2 shall clearly state that it covers lintels only for semi-structural use and an explanation is given what semi-structural role means. - Clause 5.3: Mechanical performance shall cover SLS examinations i.e. crack width (when relevant) and long term deflection. - Clause 5.3.2: The characteristic load bearing capacity for lintels shall be declared as characteristic value (confidence level 75 % and 5 % fractile). Principle of the EN 1990 shall be followed. - Clause 5.3.4: Determination method is just given for the short term deflection. However, the national requirement levels are given for long term deflection. Calculation methods have to be developed to determine the long term deflections of different kind of lintels. It is too expensive to use long term loading tests to determine long term deflection. - Clause 5.7.1: It is impossible to declare just “freeze/thaw resistant” or “not freeze/thaw resistant” since freeze/thaw resistance requirements vary in different Member States due to different climatic conditions. More specified verification method and declaration is needed. - Clause 8.3: More precise FPC rules are needed. For example testing frequencies for FPC characteristics shall be specified. There is no notified body position paper concerning lintels. - Table ZA.1: Separate tables ZA.1a, b and c are needed for single lintels (combined lintels), composite lintels and prefabricated parts of composite lintels. - Table ZA.1: All the information given in the tables 2 and 3 is related with the mandated characteristics. This shall be given in table ZA.1 as proxy characteristics. - Figure ZA.1: CE-marking example needs complete rewriting. Separate CE-marking examples are needed for single lintels (combined lintels), composite lintels. Note: Standard EN 845-2 is under review in CEN TC 125. New EN 845-2 will include improvements compared to the existing EN 845-2:2003 but it seems that the deficiencies presented above will not be solved. |  |  |
| EN 998-1:2003/AC:2005 Rendering and plastering mortar | FI Comments: More precise FPC rules are needed. For example testing frequencies for FPC characteristics shall be specified. There is no notified body position paper concerning these products. Note: Standard EN 998-1 is under review in CEN TC 125 but it seems that the above problem will not be solved. |  |  |
| EN 998-2:2003 Masonry mortar | FI Comments: Finland requests the modification of the standard. The characteristic bond strength (shear bond strength and flexural bond strength between mortar and masonry units) shall be included in the harmonised product standard. This characteristic bond strength is relevant for both the masonry units and mortar. It should be left to the manufacturers of masonry units and mortars to decide if the characteristic is declared in the CE-marking of masonry unit or in the CE-marking of masonry mortar. Note: Standard EN 998-2 is under review in CEN TC 125 but it seems that the above problem will not be solved |  |  |
| EN 12101 – 2 Smoke and heat control systems – Part 2: Specification for natural smoke and heat exhaust ventilators | Germany: Unclear and/or insufficient provisions concerning the initial type-testing after change of a product. | 2009-06-17 No information received so far from DE. CEN/TC 191 is currently working on the improvements. Revised reply to the mandate should be sent to COM. | DE considers that minor details need to be settled. Official DE reply is still expected (03/09/2009). |
| EN 12101-10:2005 Smoke and heat control systems – Part 10: Power supplies | EC services: The mandated characteristic "Performance parameters on failure of primary source (for power supplies – includes functioning time)" is not included but in fact the standard deals with this aspect under the characteristics operational reliability and response time. Durability is not dealt with at all, yet in the body of the standard it is under clauses: 12.8, damp heat – steady state; 12.9, vibration – sinusoidal; 12.11, SO2 corrosion; 12.12, salt spray testing. It needs to be included and these references be added to the table. Examples of CE marking They should indicate values against the mandated characteristics but they do not. This needs to be amended | 2009-06-17 No information received so far on the results of the check as required by the “way forward”. CEN/TC 191 position: These comments shall be handled by TC and the result brought into the next revision of this hEN together and in accordance with an amendment of the existing answer of TC 191 to M/109, as amended by M/139. | EC to check that this essential characteristic is covered by the mandate and if not to check if there are MS regulations. |
| EN 12326-1 Slates and stone products for discontinuous roofing and cladding – Part 1: product specification | EC, DA, SE: The standard covers only slates of tectonic origin. Products placed today legally in the markets of MS are excluded without justification. The standard needs to be revised to include also the above mentioned slates. | CEN TC agreed to revise the standard. Expert meeting foreseen in February 2010 |  |
| EN 12566-3:2005, Small wastewater treatment systems for up to 50 PT – Part 3: Packaged and/or site assembled domestic wastewater treatment plants. | EC services: Table ZA.1 As regards the “water tightness test” there are in fact two tests with one pass level each and two other tests with a choice of either three levels of vacuum in one case and three levels of pressure in the other (Annex A). Ultimately there are eight “pass” options. This contradicts mandate which specifies that one test should be chosen. In fact according to the table A.1, the water test in A.2 is applicable to all the products made of different materials, therefore it is difficult to understand why this test was not chosen in isolation. Similarly for the “crushing resistance and maximum load deformation”, Annex C, table C.1 lists about nine methods to determine structural behaviour whereas only one Method C.6, the “Pit test” is applicable to all materials. In addition all the other methods, other than method C.6, only produce figures to be used in national calculation procedures whilst the method C.6 determines a pass/fail requirement. Again it is difficult to understand why method C.6 was not chosen. Clause ZA.2.1 It contains an incorrect reference to the AoC Decision. It should be 1997/464/EC of the OJ 198, 25-7-1997. Table ZA.3 Assignment of evaluation of conformity tasks reflects the problems identified in Table ZA.1 above. | CEN/TC 165 position: The final draft EN 12566-3:2005/prA1:2008 has been sent to CMC on 2008-05-09 for launching a 3 month UAP. The EC queries concerning the French request are covered by this amendment. The comments of the CEN consultant have been included. | CEN: Amendment progressed |
|  | NEW : 2009-03-23 FINNISH COMMENTS Subject: Deficiencies in harmonised product standard EN 12566-3+A1 ‘Small wastewater treatment systems for up to 50 PT – Part 3: Packaged and/or site assembled domestic wastewater treatment plants COMMENTS from the Head of the Finnish Delegation to SCC General Some of the comments go beyond the role of the regulator but we believe that they improve clarity and user friendliness. Detailed comments 1 Scope Treatment plants for the treatment of pure grey water (domestic wastewater except toilet wastewater) shall be more clearly excluded from the scope of this standard. This can be done e.g. by modifying the last sentence of the first paragraph as follows: Small wastewater treatment plants according to this European Standard are used for the treatment of raw domestic wastewater except pure grey water. In addition answer to the mandate shall be modified to exclude treatment plants for the treatment of pure grey water. Justification: Treatment efficiency test method in this EN-standard is not applicable for the treatment of pure grey water. 3 Terms and definitions Definition for nominal designation shall be added, see prEN 12566-6. 6 Requirements New clause New clause 6.1.X Overall dimensions shall be added. See clause 6.1.2 in prEN 12566-6. Assessment of overall dimensions shall be done by measurement with accuracy of ± 20 mm. Clause 6.1.1 This clause gives a requirement for the treatment plant to be provided with an alarm system to indicate operational failure. However, no test method is given how to verify the operational reliability of the alarm system. Short term solution: Alarm system is excluded from the scope of the standard and from clause 6.1.1. Then requirements for the alarm system can be given nationally following the NOTE in the Scope. Long term solution: TC 165 develops operational reliability test for the alarm system of the treatment plant where it is needed. Then alarm system is included in the scope of this standard and added to clause 6.1.1. In addition the proxy characteristic ‘operational reliability of the alarm system’ shall be added to Table ZA.1 and to the answer to the mandate. Clause 6.1.2 This clause shall be part of the harmonised standard. That is why Table ZA.1 shall make reference to clause 6.1.2 with a pass criterion. Answer to the mandate shall be modified accordingly. In addition accuracy requirement shall be added, see clause 6.1.3 in prEN 12566-6. Assessment of inlets and outlets shall be done by measurement with accuracy of ± 1 mm. Assessment of internal pipework and connections shall be done by visual control. Justification: Requirements in clause 6.1.2 have to be fulfilled to ensure reliable treatment efficiency. Clause 6.1.2 Inlet and outlet pipes shall be compatible with standardized pipe systems. Clause 6.1.3 This clause shall be part of the harmonised standard. That is why Table ZA.1 shall make reference to clause 6.1.3 with a pass criterion. Answer to the mandate shall be modified accordingly. Justification: Requirements in clause 6.1.3 have to be fulfilled to ensure reliable treatment efficiency. Clause 6.1.3 The size of the extension shafts shall have a minimum dimension of 600 mm for products for which there is a need to perform maintenance inside the treatment plant. The requirements related to the volume of the plant shall be deleted. Clause 6.2.1.1 Second paragraph is not acceptable. It is not allowed to state in the harmonised product standard that the structural calculation shall be made according to calculation methods accepted in place of use especially when European calculation methods are available. This is not harmonisation. For plants made of concrete or of steel reference shall be made to EN Eurocodes which included applicable calculation methods also for treatment plants. For plants made of other materials reference may be temporarily made to calculation methods accepted in the place of use. TC 165 shall immediately start the preparation of European calculation methods for these other materials (PVC-U, PE, PP and GRP). Clause 6.5.2 Compressive strength shall be greater or equal to C 35/45, not exactly C 35/45. Reference is made to Table A.2 and A.2 of EN 13369. However, Annex A in EN 13369 is informative giving just recommended values for the concrete cover of reinforcement. The concrete covers required are given in the National Annexes of EN 1992-1-1. Clause 6.5.3 Steel parts in connection with wastewater shall be stainless steel in accordance with EN 10088-1, EN 10088-2 and EN 10088-3 and their corrosion resistance shall be at least equal to austenitic steel X5CrNi1810. Those duplex or ferrite stainless steels which have at least equal corrosion resistance as austenitic steel X5CrNi1810 may also be used. Justification: Reference to clause 6.2.3 in EN 858-1 is not correct since it covers also other steels than stainless steel. In addition minimum corrosion resistance requirement is given in clause 6.2.3 of EN 858-1 by reference to austenitic steel X6CrNi1810, which is wrong. 7 Calculation and test methods Titles of clause 7 and 7.3 are misleading since no calculation methods are given, just rules how to determine some material characteristics needed as input values in the calculation. 9 Evaluation of conformity Clause 9.2 Limit values shall be given how much tested organic daily load (BOD) may vary from the nominal organic daily load (e.g. from 65 % to 125%). Clause 9.3 Factory production rules are very short and very general. Detailed FPC rules (including FPC testing frequencies) for each material shall be prepared. This is especially needed since AoC system is 3 with no intervention of notified body after ITT. Table 2 in prEN 12566-6 could be used as a model with some adjustment. Finnish proposal for a new Table to be incorporated in clause 9.3.4 is as follows: Table X – Minimum frequency of FPC testing for prefabricated small wastewater treatment systems Annex A Clauses A.2.2, A.3.1 and A.4.1 It shall be clarified that the extension shaft or structurally similar upper part shall be included in the test sample when the connection of the upper part with the treatment plant is under ground water level. In this case the manufacturer shall declare the maximum height of the ground water level in relation to the treatment plant. Justification: Water tightness tests do not secure that water tightness is achieved against outside water pressure (when plant is under ground water level) if the extension shaft is separate part connected to the plant with a joint. Annex B Clause B.3.2 In the point c) total nitrogen (TN) should be accepted as well as Kjeldahl nitrogen (KN) and ammonium nitrogen (NH4-N). In Finland the total nitrogen is more commonly used method. We propose the following revised sentence in the point c): KN: 25 mg/l to 100 mg/l or TN: 25 mg/l to 100 mg/l or NH4-N: 22 mg/k to 80 mg/l; It should be defined in the standard what to do if the influent quality is not in the required limits. We propose the following addition after the first paragraph: During the testing the deviations from the influent limits of given parameter are acceptable if the mean value of sequence samples of this parameter is inside the limits and if the deviation is inside the accuracy of the test method. In the sequence where the mean value of sequence samples was not inside the limits additional samples should be taken so that the mean value of the sequence samples is inside the limits. Clause B.3.4.1 The following addition is proposed after the first paragraph: The order of the sequences in the test schedules is optional. Nominal, underloading, low occupation stress and overloading sequences may alternate with each other. Clause B.3.4.2 It should be defined when the measurement is taken after the overload. We propose the following sentence to be added after the first paragraph or to clause B.3.5: After 48 h overload the 1st sample shall be taken immediately after the overload and the 2nd one week from the 1st sample. Clause B.3.4.3 The method of peak flow discharge is not clear and should be clarified after the second paragraph or to clause B.3.5 as follows: The different peak flow discharges of 200 l shall be made consecutively N times (N is the number of peak flow discharges given in table B.4.) It should be defined when the measurement is taken after the peak flow discharge. We propose the following sentence to be added after the second paragraph or to clause B.3.5: After peak flow discharge a period of 3 days shall be allowed before sampling. Clause B.3.4.4 It should be defined when the measurement is taken after the 24 h power breakdown. We propose the following sentence to be added at the beginning of the second paragraph or to clause B.3.5: The 1st sample shall be taken after one week from the end of the power breakdown of 24 h. Clause B.4 Some of the measurement methods given in Table B.5 are not used anymore by the analyzing laboratories. They use modern analysis methods which are developing all the time. We propose the following sentence to be added after the first paragraph in B.4: If other analysis methods are used they should be according to ISO or EN –standards and they should be validated by the relevant sector group of Notified Bodies to ensure the accuracy and quality of the chosen methods. Annex C Title Title is misleading since no calculation methods are given, just rules how to determine some material characteristics needed as input values in the calculation. Clause C.1 Too many alternative methods for the determination of structural behavior are given in Table C.1. There is no guarantee that they give equal results. Method C.2 in Table C.1 can be used only in dry conditions. Crushing test for concrete plants does not consider the outside water pressure from ground water. This is relevant when plant is in wet condition under ground water level. Clause C.4.5 Reference to relevant standards is not acceptable. It shall be specified which EN standards can be used to obtain steel characteristics. Clause C.6.2 Pedestrian load cannot be decided by this standard. Pedestrian loads may vary since they are Nationally Determined Parameters of EN 1991-series. That is why reference shall be made to design pedestrian load of EN 1991-series with the used safety factor. Not to give a fixed value i.e. 2,5 kN/m2. Clause C.6.3 Pedestrian load used in the test shall be given in the test report and shall be declared in the CE-marking. Requirement for the variation of the volume of the plant after pit test is too large. Requirement shall be lower than 20 %, e.g. 5 % or 10 %. Annex ZA Clause ZA.1 The following proxy characteristics shall be added to Table ZA.1 (In addition the answer to the mandate shall be modified accordingly): Under mandated characteristic ´Effectiveness of treatment’: - Hydraulic design, reference to clause 6.1.2 - Access, reference to clause 6.1.3 Clause ZA.3 The following modifications are needed in item e) e) information on the relevant essential characteristics listed in Table ZA.1, as follows: - effectiveness of treatment expressed as mean treatment efficiency ratio of COD, BOD, SS, nitrogen parameters and total phosphorus obtained during nominal sequences together with the tested organic daily load (BODx) with used power consumption and the mean temperature (liquid phase) of the wastewater in the test, - nominal designation … - watertightness … - loadbearing capacity with the method used and maximum load deformation (as characteristic load bearing capacity) with dry, wet conditions, characteristic pedestrian load and the maximum embedding height and used Nationally Determined Parameters NDPs when relevant, - durability… Justification: Power consumption is required to be declared in clause 6.3. - Nitrogen parameters and total phosphorus parameters are required by the Finnish national regulations. See also clause B.2.4 where they are also mentioned. - Treatment efficiency varies considerably with the temperature of wastewater used in the test. That is why it is necessary to declare the used temperature in the CE-marking. In the standard there should be coefficients how to compare test results achieved at different temperatures. - Different test methods (see Table C.1) are used for dry and wet conditions. That is why it is necessary to declare it in the CE-marking. - Pedestrian load varies in the Member States. That is why it is necessary to declare the used pedestrian load in the test in the CE-marking. - Manufacturers are allowed to change the height of the extension shaft compared to the one used in ITT. That is why it is necessary to declare in the CE-marking the maximum embedding height. - When EN Eurocodes calculation methods are used, all the used NDPs (except recommended values) shall be declared in the CE-marking. Figure ZA.1 Example of the CE-marking shall be modified to cover the same information as required in item e) of clause ZA.3. Also with the pit test load bearing capacity shall be declared. Not just declare ‘pass’. | 2009-06-17 CEN/TC 165 position: First of all CEN/TC 165 would like to draw attention to the following facts: • EN 12566-3 has been published in 2005 taking into account the Mandate M118 and the accepted answer to the mandate. • The draft standard prEN 12566-3 was published for comments in 1999. Also Finnish experts were involved in drafting the standard. • At request of the French legislator concerning the declaration of the performance of treatment efficiency an amendment has been published in 2009. The transition period has been extended by the Commission up to 2010-07. • During the drafting process CEN/TC 165 never received such comments from the Finnish CEN member body. After publication of EN 12566-3, CEN/TC 165 continued drafting further parts of EN 12566 series for small wastewater treatment plants and published prEN 12566-6 already. prEN 12566-7 will be published soon. During the work on prEN 12566-6 and prEN 12566-7 lot of improvements have been made and new developments have been taken into account. Considering the personnel and financial resources of WG 41 as well as the time schedule for standardization projects (3 year time frame) to accommodate new WI without detriment to its work programme, TC 165 decided by RESOLUTION331/2005 (Oslo-13) taken on 2005-04- 07/08, to request WG 41 to follow strictly the WG 41 business plan where it was fixed that that work on all parts of the series EN 12566 shall be finished before new work will be started. - 2 - The remaining two projects are EN 12566-6, which will be finished in 2010 (final draft to be sent to CMC on 2010-08) and EN 12566-7, which will be finished in 2011 (final draft to be sent to CMC in 2011-04). As applicable, TC 165 will consider your comments for finalization of prEN 12566-6 and prEN 12566-7. Immediately after that work is finished, CEN/TC 165/WG 41 will start with the revision of EN 12566-3. At that stage all comments on EN 12566-3:2005 of the Finnish Head of the Finnish Delegation to SCC, as received on 2009-03-23, will be considered. EN 12566-3:2005 will be reviewed in 2010. |  |
|  | DE COMMENTS (04/09/2009): Reaction to fire performance aspects need also to be addressed by the hEN. |  | EC submitted proposal for relevant amendment of M118 |
| EN 12620:2002/A1 Aggregates for concrete | The range of application of the standard is defined wide enough so that also recycling products can come under it. But requirements concerning environmental compatibility are not defined. CEN/TC 154 will catch up on this with the next revision. Besides, until now – for lack of harmonized test methods – the property "alkali-silica reactivity" has not been harmonized yet. A European test standard has temporarily failed. DE COMMENTS: |  |  |
| EN 13108-1 to 7 Bituminous mixtures | Spain: Deficiencies have now also been found in a series of harmonised standards, EN 13108 Parts 1 to 7 dealing with bituminous mixtures. Their references have been published in the OJEU and their period of coexistence ends in March 2008. In this case the deficiencies relate to margins of tolerances for contents of soluble binder and for grading of aggregates. Such deficiencies are found when using Parts 20, regarding Type Testing, and 21, regarding Factory Production Control, to which all first seven parts make reference for evaluation of conformity and therefore of compulsory application for CE marking. Details are provided in the attached document which, as the previous one, was received from Directorate General for Roads. The reason for submitting this new query is once again incompatibility with the national regulatory bill, the same as in the previous query, in force since 1999. A copy of relevant pages of I this bill are included in the attached document and related paragraphs are shaded in colour. Translation of those paragraphs will be provided if requested. This regulation was the subject of a notification under 98/34/EC directive with reference number 1999/340/E, and the complete text is available in English, French and German in TRIS. | CEN/TC 227 position: We note the comments of Spain to SCC concerning EN 13108 Parts 20 and 21 and are somewhat surprised that these have not previously been brought up by Spain in TC 227 which is the CEN committee which produced the documents. In the process to come to a Harmonised European Standard there are many possibilities and opportunities to comment on the draft standards in the development process. The two standards in question were drafted in a very open process within the CEN committee in which the views of all member countries were actively sought and a detailed consensus position was established. The standards 13108-20 and 13108-21 were drafted over several years by a well balanced task group which included active representation from the National Highway administrations of UK, France, Germany and Denmark in addition to experts from industry. The acceptance criteria and tolerances used in many countries were examined in great depth and the standards were drafted to be as compatible as possible with established practice. After that the drafts were discussed several times in the Working Group. Then the drafts went for CEN Enquiry and in the end for Formal Vote and in each step the comments were discussed. Tolerances similar to those proposed by Spain were debated in the past in some detail but rejected and in the end TC227 came with a draft that was accepted by a large majority. In the Formal Vote process that started for prEN 13108-20 and 13108-21 on 2005-06-09 and that ended 2005-09-09 22 National members, including Spain (AENOR), approved the draft of prEN 13108-20. |  |
|  | Reaction from ES on 03/09/2009 by e-mail: Regarding the query of Spain on the European harmonized standards (series EN 13108. Bituminous mixtures) it is necessary to say: Background - In October, 2007, the Ministerio de Fomento sent a query to the SCC on the issue of the deficiencies discovered by the Spanish Directorate General for Roads in harmonised standards related with bituminous mixtures (series EN 13108) asking to be included under point 6 of the Agenda of the SCC Preparatory Group meeting held in October 8, 2007. - In November, 2007, the same document was sent again in order to be taken into account in the 66th meeting of the SCC of December, 2007. - On December 23, 2007, CEN, having been informed by the SCC of these deficiencies, released a report promising to discuss the same ones in the CEN/TC227/WG1 meeting of April 17, 2008. - In the CEN/TC227/WG1 meeting of April 17, 2008 in Reykjavik, the Spanish representative presented again the position of Spain, indicating that it had not been sufficiently understood, answering to the above mentioned report. In this intervention, he mentioned that Spain could agree with the part concerning tolerances but that DG Roads maintained its position on the part concerning the analysis of sensibility. Such observations were not included in the minutes of the meeting. - In July, 2008, a letter was sent to the SCC to which a report of Directorate General for Roads justifying the position of Spain in the same terms as summarized in the previous point is attached. - In the CEN/TC 227/WG1 meeting of October 27-28 in Zagreb, the Spanish representative requested the modification of the minutes in order to include the observations of Spain. - Finally, in the 68th meeting of the SCC of November, 2008, the Spanish representative raised again the query of Spain with regard to the series of harmonized standards EN 13108 . The above mentioned request was not included in the minutes of the meeting. In the 69th meeting of the SCC of June, 2009, the Spanish representative requested that the minutes of the previous meeting be corrected in its point 12 in order that the query of Spain is included. Conclusion The technical specifications of the Spanish roads regulation, in force since the year 2004 by means of the ministerial Order FOM/891/2004, of March 1, and of obligatory fulfilment in Spain, were not taken into account in the drafts of the harmonized standards. This regulation was the subject of a notification in conformity with the 98/34/EC directive, being the complete text available in English, French and German in TRIS as dossier 2003/102/E. As for the comment from CEN/TC227/WG1 reminding that AENOR (Spanish NSB in CEN) did not rise observations in the formal vote process of prEn 13108-20 and prEN 13108-21 standards, it is necessary to say that AENOR develops its activity in the private area, whereas the ministerial Order FOM/891/2004, of March 1, concerns the Spanish legislation and is approved by the Government. Since the Government of Spain had news of the content of the series of harmonized standards EN 13108, it has been reporting, both to the SCC and to CEN the existence of the national regulation that since the year 2004 has been establishing the mentioned technical specifications, without, up to the moment, being taken into account. We once more insist in the need to modify the series of harmonized standards EN 13108 in order to allow the fulfilment of the ministerial Order FOM/891/2004 just as it has been reported both in the SCC and in the CEN, through TC 227/WG1. Attached pleased find the report of of Directorate General for Roads justifying the position of Spain about deficiencies discovered in harmonised ENs 13108. Bituminous mixtures. Material specifications. Same report was previously sent 17/07/08. |  |  |
| EN 13162 “Thermal insulation products for buildings - Factory made mineral wool (MW) products – Specification” to EN 13171 | Comments on harmonised standards for thermal insulation products i.e. EN 13162…EN 13171 Note: Especially comments are prepared for EN 13162 Thermal insulation products for buildings – Factory made mineral wool (MW) products – Specification 1. Solutions needed in the short term 1.1 Declared values for thermal resistance and thermal conductivity The rules how to determine declared values of thermal resistance and thermal conductivity should be clarified. In the Annex A it has been written correctly that it is the responsibility of the manufacturer to determine the declared values of thermal resistance and thermal conductivity. However, clause 4.2.1 and also Annex D give an other interpretation. The declared value of thermal conductivity shall not be the calculated value λ 90/90 after rounding upwards to the nearest 0,001 W/(mK) using the step of 0,001 W/(m K) from ITT tests as it can be now understood from the standards. The declared value of thermal insulation resistance shall not be the calculated value R 90/90 after rounded downwards to the nearest 0,05 m2 K/W from ITT tests as it can be now understood from the standards. The manufacturer has to determine the declared values based on evaluation of ITT test results. The declared values must be on safe side compared to the calculated λ 90/90 or R 90/90 values from ITT population of samples. Then in continuous factory production control the manufacturer has to show that the calculated λ 90/90 or R 90/90 value from FPC population are in the limit of the declared value (on the "safe" side). There should not normally be a need to declare other new declared values when mean values and variations of results are regularly calculated for FPC population according to Annex A. 1.2 Influence of air flow resistance (convection) to the thermal resistance/conductivity (only relevant for EN 13162) It is a physical fact that convection will increase considerably the thermal resistance and decrease considerably thermal conductivity of thick insulation layers in the building envelope. Nowadays it is not possible to take this phenomenon into account in design since CE-marking of mineral wool does not normally include information on its convection behaviour i.e. its air flow resistance. This characteristic is only declared in the CE-marking if product is used for sound insulation applications. That is why it is necessary to add into Table ZA.1 in EN 13162 a third proxy characteristic ‘air flow resistance’ under the mandated characteristic ‘Thermal resistance’. In this way it is possible in national rules (for the determination of design thermal resistance/conductivity from declared values) to take convection in account by using only CE-marking information as input values of the calculation. There is no need to modify the mandate M102. TC 88 answer to the mandate just needs updating. 2. Solutions needed in the long term 2.1 Harmonised product standards for thermal insulation products taking into account the intended end use of the product Harmonised product standards for thermal insulation products have been prepared to cover all kind of end uses. Normally the manufacturers just declare in the CE-marking that their products are intended of all applications in the building. Unfortunately this means that the harmonised product standards for thermal insulation products do not take into account the specific regulatory needs of different end use applications of thermal insulation products. For example thermal insulation may be fixed on the roof by using mechanical fixings. Existing harmonised product standards do not include any characteristic which could give information if the product is applicable to be used with the mechanical fixing and which kind of forces can be transferred. Harmonised product standards should be further developed to handle the different end use applications of thermal insulation products i.e. separate Tables ZA.1 for different end-use applications are needed to the harmonised product standards. Note: For many other construction products (See e.g. EN 12602 ‘Prefabricated reinforced components of autoclaved aerated concrete’) this kind of approach is already in use. TC 351 has made a conclusion that before dangerous substances can be covered in harmonised product standards the intended use of the product has to be specified more accurately than nowadays in the CE-marking. 2.2 Determination of design thermal resistance or conductivity Declared thermal resistance/conductivity values are given in the CE-marking. These declared values cannot be used in the design of structures since they do not take into account the practical and long term conditions of thermal insulation products in different end uses. Design thermal resistance/conductivity values are used in the calculation of energy efficiency of buildings. Design thermal resistance/conductivity values are nowadays determined from declared thermal resistance/conductivity values using national calculation methods. It would be beneficial for the internal market of construction products if European guidance (e.g. EN-standard) is developed to help the Member States to give coherent rules for the determination of design values from declared values for different insulation materials. |  | EC to send letter to TC 127 for the assessment of "glowing combustion" performance |
| EN 13747:2008 “Precast concrete products - Floor plates for floor systems” | 2009-03-23 Comments on the new amendments to the harmonised product standards of precast concrete products I refer to the minutes of the meeting held on 23rd of April 2008 where I was asked to make these comments. I have also wanted to give the reasons why I feel it necessary to make these comments. 1. Background Finland sent comments (20th of February 2006) on several harmonised product standards (including also precast concrete standards) to the Eurocodes National Correspondents group. Finland expressed that these precast concrete standards did not fulfill the requirements of Guidance Paper L. E.g. there were no separation between Methods 3a) and 3b). After that TC 229 started to improve its standards by taking into account also the Finnish comments. We appreciate that. But the new amendments are not totally acceptable. My comments are based on the study on EN 13747 Precast concrete products – Floor plates for floor systems, its amendment prA1 (March 2008) and EN 13369 Common rules for precast concrete products. Comments are probably also valid to all new amendments prepared by TC 229 since they are based on the same model. See amendment prA1 of EN 13747 enclosed in Annex 1. There are inconsistencies between interpretation of Guidance Paper L CE-marking methods in hENs for structural products prepared e.g. by CEN TC 124, TC 135, TC 177 and TC 229. Common approach is needed. 2. Detailed remarks on EN 13747/prA1 ZA.3.2 (Method 1) No guidance is given how to declare the harmonised characteristic durability. The basic idea of the CE-marking to declare the harmonised characteristic in a comparable way between different manufacturers is not achieved. ZA.3.3 (Method 2) Declarations of serviceability limit state aspects (cracking and deflection) are missing from Figure ZA.3. This shall be part of the harmonised characteristic mechanical strength as explained in the Annex 1 of the CPD. In Finland we have serviceability limit state requirements in our regulations. No guidance is given how to declare the harmonised characteristics geometrical data, detailing, durability, acoustic insulation parameters, complementary information on fire resistance and other NDPs. The basic idea of the CE-marking to declare the harmonised characteristic in a comparable way between different manufacturers is not achieved. Term ‘Position number’ in Figure ZA.3 should be clarified. In Method 2 it cannot mean the location of the precast concrete unit in the works. ZA.3.4 (Method 3a) These are so called made to measure products produced according to a specific client’s order and where structural design of the product is outside the CE-marking. Structural design is performed by the purchaser or by the manufacturer in cooperation with the purchaser. When fixing the CE-marking on the product the manufacturer just declares that he has produced the product according to the production drawing (e.g. used the materials specified in the production drawing). Structural design can be performed according to any (national) design code but it is not part of the CE-marking. Clear reference to the production drawings (number and date) are missing in Figure ZA.4. Reference to the client’s order is also needed if it is not given in the production drawing. Figure ZA.4 can be simplified since there is no need to declare geometrical data and detailing in the CE-marking since they are already given in the production drawing. In addition the manufacturer cannot declare mechanical strength, fire resistance, acoustic insulation parameters and durability in the CE-marking since in this method those characteristic shall be considered outside the CE-marking e.g. by the client. ZA.3.5 (Method 3b) These are so called made to measure products which are produced for a specific works and where structural design of the product is part of the CE-marking. We cannot accept that "This method applies also in the case of a structural design made with means other than EN Eurocodes". This is an important safety issue. Our arguments are the following: Generally mandated characteristics can be declared based on testing or calculations as specified in the relevant harmonised product standard (hEN). In hENs reference is made to the European test methods given in EN-standards. It is not acceptable to write in hENs that testing can be made by means other than by test xxx determined in standard yyy. In the CPD there is nothing which gives a right to treat calculations differently than testing. The tasks and duties of notified bodies have been mentioned in Guidance Paper K and Guidance Paper A. Notified bodies are recognized to be competent by Member States. The competence is based on the CPD, Guidance Papers and relevant hENs. Notified bodies have to understand required tests and calculations rules. Building authorities cannot demand anything else as mentioned in CE-marking. Finnish building authorities cannot accept imported construction products for structural use which have been calculated according to national design rules as part of the CE-marking. Criteria for the notified bodies verifying structural design calculations of the products do not include the knowledge on the national design codes of all 27 Member States. But they include the knowledge on the Eurocodes. Method 1 and 3a are for those cases where national design codes are used but then calculations are outside the CE-marking. These calculations are treated and checked according to national practices valid in the country where the product will be used. No guidance is given how to declare the harmonised characteristics geometrical data, detailing, mechanical resistance, fire resistance, acoustic insulation parameters and durability. The basic idea of the CE-marking to declare the harmonised characteristic in a comparable way between different manufacturers is not achieved. In Figure ZA.5 reference to the client’s order shall be replaced by specifying the works and the position number of the product in the works. 3. General remarks Attestation of conformity procedures for structural construction products It is up to CEN TC to decide which methods of Guidance Paper L are to be introduced in each hEN for structural products. Sometimes only method 1 is valid e.g. for sawn timber. Normally it will be useful to have all methods since it is difficult to know which methods may be needed in the future. It is important to understand that the attestation of conformity tasks is different for different GP L methods. These tasks have been described in hENs in Table ZA.3 –Assignment of evaluation conformity tasks. This table is difficult to understand and do not give detailed information to the manufacturers and the notified bodies. I think that it would be more useful to have separate tables for each GP L method. Harmonised product standards shall describe more in detail the tasks of the manufacturers when performing the structural design calculations and the tasks of the notified bodies when verifying these calculations according to Guidance Paper K. I refer to Guidance Paper K where it has been explained that calculations can be a part of Initial Type Calculations (long series) or "calculations performed on individual manufactured product may be part of the factory production control in analogy to testing of samples taken at the factory" (small series). Method 2 is usually for long series products where production can continue years based on the same calculations. Then it is wise that notified body "checks" these calculations. Methods 3a and 3b relate to small series production. It is impossible that the notified body will "check" all calculations which have been carried out by the manufacturer. But the notified body can "check" some calculations in analogy to testing of samples at the factory. In the case of small series "checking of calculations" can be also a task of the inspection body. I refer to the Annex III of the CPD "inspection body, …. such as assessing, recommending for acceptance and subsequent audit of manufacturers' quality control operations, and selection and evaluation of products on site or in factories or elsewhere, according to specific criteria;" The problem is that the hENs for precast concrete products do not give detailed instructions how to carry out the tasks and duties which relate to calculations mentioned in Guidance Paper K. In many cases GP K states "in accordance with the provisions of the hEN". But in many cases there are no provisions or only very general provisions in the hENs. We think that this is not acceptable. It shall be described in the same detailed way as for testing. We have to be able to rely the manufacturers and notified bodies carry out these tasks and duties in a coherent way. These tasks and duties cannot vary very much from one Member State to another. It is credibility issue for the CE-marking and it is also a safety issue. Service limit state requirements In Finland we have service limit state requirements in our regulations. These service limit state requirements are not in Annex ZA. These shall be added. 4. Long term objectives (valid for all harmonized product standards for structural products) 4.1. User friendliness of standards and coherence of harmonised standards for structural use Harmonised product standards refer to technical information, technical documentation, design specification etc. The content of these terms have not been defined coherently between harmonised product standards for structural use. In Annex M of EN 13369 there are some explanations. Harmonised product standards should be such that these are easy to understand and these can be understood in the same way. The content of these definitions shall be determined more in detail. 4.2. Attestation of conformity for calculations Attestation of conformity decisions are based on article 13.4 of the CPD. There is nothing in the article which relates to the risks related to the calculations (for structural use). There are attestation of conformity decisions 1; 2+ and 3 (seldom) for products for structural use. But the risks related to the calculations may be the same. In some cases we can conclude that the risks related to the calculations are less for some AoC 1 products than for some AoC 2+ products. The CPD shall treat fairly manufacturers. The requirements shall be based on objective reasons. It would be useful to have additional criteria for the risks related to the calculations and to determine the attestation of conformity systems for calculations in some new way. | 2009-06-17 CEN/TC 229 Chairman: I am very happy to see that M.J.Virtanen recognizes that new Annex ZA (that we generalize) provides a great improvement. Now he sends us new comments, I can understand some of them as general, others are the result of M.J.Virtanen's personal interpretation. I will try to answer to each comment by reference to our last model of Annex ZA. - ZA.3.2 (Method 1): in ZA 3.2 it is written "provisions for durability", I recognize that it is not a guidance but "durability" is presently a NDP so it is was not possible to be more precise. When common rules will exist on that item, we will apply them. -ZA.3.3 (Method 2): Serviceability limit state aspects are mandatory in Finland, but not in all Member States! So they are NDPs and reference to NDPs is made in the text. I agree that it is not given any common declaration method for the items listed by Matti. The term "position number" is probably not exactly the best. -ZA.3.4 (Method 3a): reference to design specifications is mentioned in Figure ZA.4 and traceability is covered by FPC. I do not understand how figure Z.A.4 can be simplified as the characteristics mentioned there are explicitly required by the Mandate. About the addition mentioned by Matti, it does not cover items declared by the producer, it is only an information to indicate where they can be found. -ZA 3.5 (Method 3b): Use of other design methods than Eurocodes is explicitly allowed (as a transitional possibility) by GP L 3.3.4. Moreover, as far as I know, criteria for Notified Bodies do not include the knowledge of Eurocodes and for AoC system 2+ it not their task to check the calculations: their task is (for method 3b) to check whether the calculation is covered by FPC (including Initial Type Calculation) and documented or not (we had long discussions in SG13 about that point). Reference to client's order is fundamental, works and position number are part of the product traceability and covered by FPC. -3 General remarks: 3.1: attestation of conformity procedures: I already answered. For Aoc 2+, the NB has only to check that calculations under M2 and 3b are covered by FPC. 3.2: service limit state: it is a Finnish national requirement. 4 Long term objectives: In CEN/TC229 we try to improve continuously our standards. Now we are revising Common Rules (EN 13369). About calculations, the topic is not so simple: the responsibility of the producer should be the same for calculation as for tests. | EC to send a letter to CEN asking the TC to consider durability aspects |
| - EN 14080:2005 Timber structures – Glued laminated timber – Requirements | EC services: A couple of mandated characteristics are missing from the Table Z.1. The first is dimensional stability although there is a number of long-term loading and creep tests in the body of the document which would probably suffice if referenced. The second omission is the complete disregard of the mandated characteristic "resistance to fire", there is no reference to it in table Z.1, nor any mention of the subject in the body of the standard. | 2009-06-17 CEN TC 124 has agreed in its previous TC plenary meeting (2009-05-06) on the content of the new answer to the mandate. According to the new answer to the mandate the characteristics ‘dimensional stability’ and ‘resistance to fire’ will be included into revised EN 14080. According to the new answer to the mandate revised EN 14080 will be available 2011-06. | Revised TC reply to the mandate was sent to MS for consultation EC acceptance pending. |
| EN 14081-1:2005 Timber structures – Strength graded structural timber with rectangular cross section – Part 1 : General Requirements | EC services: 1. Two characteristics which are identified in the mandate M112 are missing: - "Dimensional stability", which is not mentioned in the body of the standard nor Annex ZA and - "Resistance to fire", which is also neither dealt with in the body nor Annex ZA of the standard. This second characteristic is a particularly important one for structural elements and is a serious omission. 2. The CE marking label, shown in clause ZA.3.2, figure ZA.1, is not in compliance with Guidance Paper D, in that it does not indicate the last two digits of the year it was affixed, nor the number of the standard nor the EC Certificate number. It does however, contrary to the Guidance Paper, include the code letter ‘M’ (for machine grading) and ‘Dry graded’ if appropriate. If this is the minimum CE Marking, the last two digits of the year it was affixed and the number of the standard are required Further to the observations in the Commission’s document from 28 September 2007, some Austrian small enterprises face severe difficulties in applying the CE-mark on the product as given in EN 14081-1. They consider it unnecessarily cumbersome to mark every single piece of timber. Moreover there seem to be some confusion with the assignment of evaluation of conformity tasks to manufacturer and notified body. AT / BE / DE: Very expensive CE marking | 2009-06-17: CEN TC 124 has agreed in its previous TC plenary meeting (2009-05-06) on the content of the new answer to the mandate. According to the new answer to the mandate the characteristics ‘dimensional stability’ and ‘resistance to fire’ will be included into EN 14081-1. According to the new answer to the mandate revised EN 14081-1 will be available 2011-12. CEN/TC 124 is taking into account the EC comments in the revision of the standard. 2009-06-17: Published in 2006, EN 14081-1 is the technical specification that will be used by manufacturers to CE mark their products by September 2009. Currently, a revision of this harmonised product standard is being drafted where the discussion is focused on which pieces need to be CE marked and which do not. This discussion is going for some time and still is unresolved. It is foreseen that without guidance from higher CEN levels it leads to an undesirable situation. In the current version of the standard each single timber piece needs to be CE marked. However, an exception is made for those pieces used for aesthetical reasons when this reason is validated by the notified body. In addition, the proposed revision of the standard will also allow CE marking by batch on condition that the timber is sold directly to a specific end-user and is subject to a written agreement between the manufacturer and that end-user. The choice between CE marking by batch or piece by piece creates difficulties within CEN/TC 124 due to absence of consensus and guidance. It is the opinion of some members that CE marking of each single piece must be mandatory for the following main reasons: - there is a risk of mixing products with different technical specification on the building site - wood products need reliability to compete with other materials - piece by piece marking is technically easy especially when wood is dried and dried products are necessary for structures to avoid any serviceability and safety problems - if exceptions is tolerated for manufacturers they will never go to a piece by piece marking - if marking or no marking by piece are possible, that would create unfair competition (piece by piece marking is more expensive than by batch) - batch marking would create confusion on the markets - piece by piece is needed to secure traceability and consequently secures structural safety of buildings (use the correct product at the right place) Some members believe that CE marking by batch must always be possible for the following main reasons: - there is no regulation in any member state concerning marking of products - piece by piece marking will be problematic for the small and micro enterprises, which represent 90% of this industry (piece by piece marking needs at least half time equivalent man year), the extra cost can only be supported by big size companies - some technical problems exist to mark wet timber especially when treatment is used - there is no need to mark each product because the timber may be re-cut on site - there is no risk of mixing different qualities of wood on site (carpenter generally use the same timber grade (quality) for the required structural elements from one or more batches) - there has been no major problems with the current situation (no marking at all on the products themselves) - CPD philosophy is to allow easy access to the market by producers, while piece by piece marking requires extra costs that will result in the opposite Many discussions have been engaged within CEN/TC 124 and CEN/TC 124/WG 2 but no consensus could be reached. A clear position and guidance in this matter from a higher level is felt necessary to progress with the revision of the standard. 2009-06-17: The issue of CE marking was discussed at a special meeting with the Commission Services and the three CEN Consultants. The Commission Services supported the idea to allow both piece by piece and batch markings. | EN to be revised to solve cost problems in the standard . National annexes are not allowed in hENs. |
| EN 14190:2005 Gypsum plasterboard products from reprocessing – Definitions, requirements and test methods | EC services: Table ZA.2 - It fails to address "Resistance to fire" - The footnote to Table ZA.2 refers to Commission Decision 2003/43/EC which only refers to timber and related products. A better reference would have been Commission Decision 2003/593/EC, further updated by Commission Decision 2006/673/EC. Table ZA.3 - It indicates System 3 for all reaction to fire aspects, even if proxy characteristics are used by the notified body to assess it. - Fire resistance is missing. | 2009-06-17 Concerning "Resistance to fire", the CEN/TC 241 position is that it is not possible to include fire resistance in the standards - because fire resistance shall be measured on works and not on gypsum plasterboards only. That is why fire resistance is not included in gypsum product standards at all. A first answer on this subject has been sent to Mr. Philippe JEAN on 28-05-1997 2009-06-17 The changes required will be the subject of the next amendment to the standard. | EC closing reply to CEN pending |
| EN 14250 Timber structures – Product requirements for prefabricated structural members assembled with metal plate fasteners | Finland: In autumn 2006 Finland asked the Commission to withdraw EN 14250 from the OJ due to many deficiencies. Main reason was the wrong interpretation of GP L Methods. SCC decided to extend the CE-marking co-existence period until 1.6.2008 so that TC 124 can improve the standard. So far no agreement has been achieved in TC 124 how to modify the text concerning GP L Methods. We are afraid that there is no revised standard on June 2008. In clause 5.1 (not in Annex ZA) three alternatives are given how to declare structural characteristics: - Alternative 1) is similar to GP L Method 1. - Alternative 2) refers to national design documents, when GP L Method 2 refers only to EN Eurocodes. - Alternative 3) is similar to Method 3, but no explanation on difference between Method 3a and 3b. CE-marking examples are missing for Methods 1, 2, 3a and 3b in Annex ZA. Germany has made a notification to the Commission informing that national approval is needed in addition to CE-marking for specific timber products including prefabricated structural members assembled with metal plate fasteners. | 2009-06-17: CEN TC 124 has prepared a new draft prEN 14250 which is in accordance with the Finnish interpretation on the Guidance Paper L CE-marking methods. The draft standard is under preparation to UAP-vote in CEN CMC (2009-07). The Notified Bodies Sector Group is preparing a Position Paper including the main changes in prEN 14250 as a temporary solution for use from the end of the CE-marking coexistence period (1.7.2009) before the standard is published in OJEU. | Issue closed |
| EN 14411:2006 “Ceramic tiles - Definitions, classification, characteristics and marking” | POLAND: l. A reference to the standard EN 14411:2 006 on ceramic tiles has been published in OJ on the 4 December 2007. This standard is replacing the previous one, i.e. EN 14411 :2003 and in the Communication of the Commission there is a note in the last column stating that validity of the EN 14411:2 003 has expired on 30.06.2007. It means that there was no basis for the manufacturers to affix CE marking on these products in the period from 1 July 2007 up to the 4 December 2007. This lack of continuity of the reference harmonized standard available poses a serious problem to the producers of those products with placing them on the market, since market surveillance authorities, acting in accordance with the regulations, deny legality of such CE marking and refuse to accept it. 2. Besides, the new scope of the standard E N 14411:2006 has excluded a number of products which were previously covered by the standard EN 14411:2003 (such as edges, corners, skirting, capping, coves, beads, steps, curved tiles and others). Since all ceramic tiles are covered by the mandate M119 (see annex 1) there is a need to decide, whether or not the excluded products are foreseen to be harmonized, however if a new standard will not be prepared for them the products will be excluded from the CPD. | 2009-06-17 RESOLUTION 07/2008 taken by CEN/TC 67 on 2008-10-30 Subject: CEN/TC 67 – Italian proposal for the addition of a new WI on ceramic mosaics, trims and special ceramics components CEN/TC 67 resolves to add a new WI on ceramic mosaics, trims and special ceramics components. Scope: This European Standard specifies requirements for ceramic mosaics, trims and other special components used for floor and wall coverings, and not covered by EN 14411 (ISO 13006). | The issue of already CE marked products placed on the market needs still to be clarified. EC to send letter to EN discouraging such unilateral initiatives |
| EN 14604:2005 Smoke alarm devices | EC services: ZA.1 All the characteristics listed in Mandate M109 are dealt with except for the characteristic "Safe containment of radioactive sources". The reason for ignoring this characteristic is contained in a note to the Scope which says that "The national requirements for radiation protection differ from country to country and they are not specified in this document. Such smoke alarms should however comply with the applicable national requirements". In the spirit of harmonisation and approximation this item should be re-visited. In the second column of table ZA.1, under the heading "Clauses in this European Standard" a number of clause references is given. It is suggested that clauses 4.12 and 4.18 are not relevant in row 1. Similarly clauses 4.1, 4.2, 4.3 and 4.19 are not relevant to row 2. | 2009-06-17 CEN: Amendment to original answer being progressed CEN/TC191 position: The query is being considered by CEN/TC191 and will be reflected in the revision of the standard. | CEN TC expected to amend its reply to the mandate and to send it to EC for approval. |

QUERIES CONCERNING CANDIDATE hENs

| EN TITLE | COMMENTS | CEN POSITION | WAY FORWARD |
| --- | --- | --- | --- |
| prEN 1013 Error: Reference source not found | The French authorities consider that Standard PrEN1013 should take more account of Mandate 122 (concerning the establishment of harmonised standards for roof coverings, roof lights, roof windows and ancillary products) and particularly of the essential requirements regarding health and safety. Account should be taken of the resistance of roofing sheets to the soft impact corresponding to a person walking normally on the roof and accidentally tripping and falling for a variety of reasons, it being assumed that the sheets were fitted in accordance with the conditions governing their intended use when they were first placed on the market. It should be pointed out that the failure to take account of Mandate 122 and Article 5.1 of the construction products Directive (CPD) has already led the French authorities to make a formal objection concerning safety in the use of fibre-cement profiled sheets in accordance with Standard EN494 of 2004. It would be desirable, therefore, if some thought were given to the organisation conditions with a view to avoiding problems of "non-quality" with PrEN 1013 similar to those encountered with EN494. This was mentioned as long ago as 14 May 2008. The note to Table ZA.1.1 and the addition of an Article 5.8.2. can not be regarded as an adequate response to the seriousness of the situations arising. Note at the end of Table ZA.1.1 : “a Soft body impact resistance depends highly on the method of installation. Soft body impact resistance of a fully installed assembly/kits shall be declared separately by the manufacturer or designer of assembly/kits as stated in 5.8.2 where subject to regulation, otherwise "NPD" may be declared.” 5.8.2 Soft body impact resistance “The method(s) of installation shall consider the resistance to soft body impact. In the absence of a European test method and where subject to regulations, the soft body impact resistance may be assessed separately in accordance with the requirements of ETAG 010 or individual national safety requirements.” Similarly, it should be borne in mind that ETAG 010 refers to Standard EN15057:2006 in connection with the description of these same tests. With this type of material, however, tests with a soft object are not sufficient, since account needs to be taken of the aging of the materials, which very rapidly – in less than five years – lose their resistance to soft impacts. Finally, the question should be examined of how the danger of people falling could be indicated explicitly in the CE marking by means of a specific logo or pictogram. |  |  |
| EN 1090-1 Execution of steel structures and aluminium structures – Part 1: Requirements for conformity assessment of structural components | FINLAND: Finnish TC 135 mirror committee has decided to vote against the standard. One of the reasons is a wrong interpretation of GP L Methods. GP L Methods 1, 2, 3a and 3b are introduced in Annex ZA. Method 2 (clause ZA.3.3) refers only to EN Eurocodes but it seems to be for made to measure products, since load situations are known. No declared resistance or load bearing capacity values are given. Instead of the declared values of the NDPs the Member State (which NDPs are used) is declared. Method 3a (clause ZA.3.4) is for the case when structural design of the component is made by others than the manufacturer. However, the component specification can be prepared by the purchaser in cooperation with the manufacturer. Note: This means that also the manufacturer can make the structural design calculation outside CE-marking for made to measure products. In this case the structural design could to be checked for example by local construction surveillance authorities. Method 3b (clause ZA.3.5) is for the case when structural design of the component is determined according to the purchasers order. In addition it is explained that the structural design as part of the CE-marking can be performed according to any design specifications (e.g. according to national building codes). | 2009-06-17 Finnish appeal on EN 1090-1 is now settled so that the standard will be published with minor editorial modifications. EN 1090-1 (which will be published soon) will not satisfy the Finnish regulatory needs. That is why TC 135 will start the preparation of an amendment to consider the remarks of the Finnish appeal. For the preparation of the amendment coherent interpretation of the Guidance Paper L CE-marking methods is needed. This would require refining of the interpretation of the GP. | 1) FI to send details on still outstanding issue 2) Meeting with TC250, FI, SE, DE, EC to be organised. |
| EN 1090-2 Execution of steel structures and aluminum structures – Part 2: Technical requirements for the execution of steel structures | SWEDEN: Sweden votes no because some of the essential tolerances are too wide to be compatible with the resistance in EN 1993. Tolerances D.1.1 no 4, 5 and 6 are too wide for stocky plates compared to the resistance of a plate under compression according to EN 1933-1-5, see Annex 1. The functional tolerances should in our view not be wider than the essential tolerances. As an example D.2.5 no 1, 2 and 3 are wider than the essential tolerances for plates thinner than 5 mm. D1.3 no 1 and 2 are much wider than current Swedish tolerances and they are not compatible with the resistance of a stocky flange in compression. An example for a flange at the limit of Class 3 is shown in Annex 2. | A WG of the TC was established to consider SE query | TC results expected |
| EN 10138 – 1 Prestressing steels - Part 1:General requirements | GERMANY: The standard contains an opening clause according to which also others than the prestressing steels stated in detail in the standard can be included with other diameters and higher strengths, provided their product properties are verified according to the criteria described in the standard. However, experiences do not exist for these prestressing steels; that is why there are doubts concerning the unconditional application of the provisions of the standard to such prestressing steels. There is the danger that when applying the opening clause future prestressing steels come under the field of application of the standard, which do not show the necessary performance characteristics to guarantee the stability of the construction works according to the essential requirement N° 1. PORTUGAL: Following the discussion held at the last PG meeting on the 7th March on the inadequacy of some statements in pr EN 10138 part 1, on prestressing steel, related to its content (issue raised by the German delegation under item 11 at that meeting), I would like to confirm the Portuguese position expressed at that meeting, seconding the German reservations. This position is coincident with the opinion of the Portuguese representative to the ECISS/TC19/SC2, expressed at its meeting held on the 18th and 19th January 2007. The second paragraph of the scope of prEN 10138 part 1 means that the standard can be applied to other pre-stressing steels not covered in Annex A. This is an opening clause that can’t be accepted by Portugal. From the Portuguese point of view, this standard shall only refer to the product families prescribed within its annex A. For product families which are not stated in the standard, an ETA should be required, as far as they would be considered deviating from those ones to which the standard directly applies. So we consider: - that the second paragraph of the scope of prEN 10138 part 1: “This specification may also be understood to cover other nominal diameters and/or higher technical (strength) classes of uncoated high tensile strength steel products whose details are not stated in this specification or Annex A but whose properties and evaluation and control are carried out consistent with those specified herein.”, must be deleted; - the note of annex A: “Other product families based on steel name and/or nominal diameter are permitted in addition to those listed in Table A.1.”, must be deleted. | 2009-06-17: There has been agreement at the level of the SC with support from Germany and Portugal. The draft standard is now progressing to Formal Vote. | Issue closed |
| EN 10337 Zinc and zinc alloy coated prestressing steel wires and strands | GERMANY: Concerning the use of zinc and zinc alloy coated prestressing steel wires and strands in concrete, there is a lack of sufficient experience. Meaningful documents which make an assessment of the product possible and, if necessary, the drafting of regulations for design and execution of works by using this product, are not available. During curing the zinc coat of the prestressing steel reacts with the surrounding concrete accompanied by hydrogen evolution. The hydrogen can cause stress corrosion of the prestressing steel. Due to the EG-Guideline 53/2003/EC since 2005 in Europe mostly cement is used which contains less than 2 ppm chromate. The chromate reduction in concrete leads to a higher evolution of hydrogen. In addition the evolution of hydrogen causes a structural change of the concrete in connection with the prestressing steel which can influence the bound behaviour of the prestressing steel. Like EN 10138 this standard contains an opening clause in the definition of the field of application and in Annex A according to which also other prestressing steels not listed in the standard with higher strengths and other diameters are included in the standard provided their product properties are verified according to the criteria described in the standard. There are doubts concerning this opening clause, because experiences do not exist with the new prestressing steels. Therefore there is the danger that when applying the aforementioned opening clause future prestressing steels will come under the scope of the standard, which do not show the necessary performance characteristics to guarantee the stability of the construction works according to the essential requirement N° 1. | 2009-06-17: There has been agreement at the level of the SC with support from Germany. The draft standard is now progressing to Formal Vote. | Issue closed |
| EN 12602 Prefabricated reinforced components of autoclaved aerated concrete | GERMANY: For the verification of the properties of the construction component design or testing are foreseen and standardized in the harmonized product standard; reference to the Eurocodes is not possible. When verifying by testing according to Annex B (indirectly referred to in Annex ZA) the necessary level of protection will not be attained (statistical analysis of the tests and determination of the characteristic values are missing). This Annex B will be excluded if necessary with the national transposition. FINLAND: 2009-06-12 Finland has the following technical reservations on EN 12602 based on the information given by Finnish experts: - In Clause 4.4 reference is made to EN 12269-2 which includes a test method for long term bond between reinforcement and AAC. Test according to this published test method are impossible to perform since testing room shall be kept on 50°C for one year. A new test method is under preparation in CEN/TC 177/WG3. It should be used for the CE-marking of these products. - In Clause A.4.1.3.2 calculation equiations (A.10) and (A.11) for shear capacity of AAC beams seem to be in some cases on unsafe side. This may cause serious safety problems. Calculations equations shall be improved. | 2009-05-06 At the plenary meeting of CEN/TC 177 held on 27-04-2009 the following resolutions were passed to respond to the queries from Germany and Finland. RESOLUTION 123 taken by CEN/TC 177 on 2009-04-28 Subject: CEN/TC 177 – Answer to the consolidated queries on candidate harmonized standard (EN 12602:2008 "Prefabricated reinforced components of autoclaved aerated concrete") In order to achieve the publication of EN 12602:2008 "Prefabricated reinforced components of autoclaved aerated concrete" in the Official Journal as soon as possible CEN/TC 177 "Prefabricated reinforced components of autoclaved aerated concrete or lightweight aggregate concrete with open structure" prepared the following answer to the queries received from CMC (CEN/TC 177 N 355): "CEN/TC 177 has considered the queries on the harmonized standard EN 12602:2008 "Prefabricated reinforced components of autoclaved aerated concrete". CEN/TC 177 confirms that EN 12602:2008 covers all safety requirements based on the mandate giving the possibilities for the assessment of the characteristic mechanical resistance by calculation and by testing. CEN/TC 177 considers that also in Germany the required level of protection will be attained since safety factors can be determined nationally. CEN/TC 177 agrees that some modifications according to the German comments could be made (see Resolution 124) in order to clarify the text. CEN/TC 177 considers based on the information from the Finnish delegate that there are no problems with the Finnish authorities concerning the interpretation of Guidance Paper L methods 1, 2, 3a and 3b in EN 12602:2008. The decision was taken by unanimity. RESOLUTION 124 taken by CEN/TC 177 on 2009-04-28 Subject: CEN/TC 177 – Amendment A1 to EN 12602:2008 "Prefabricated reinforced components of autoclaved aerated concrete" CEN/TC 177 "Prefabricated reinforced components of autoclaved aerated concrete or lightweight aggregate concrete with open structure" asks WG 1 "Prefabricated reinforced components of autoclaved aerated concrete" to start work on preparing a first working draft for an amendment A1 to 12602:2008 "Prefabricated reinforced components of autoclaved aerated concrete" to address the comments of Germany and Finland according to Doc. CEN/TC 177 N 355. The decision was taken by unanimity. | Meeting to be organised with DE, FI, TC, EC |
| prEN 13172 Conformity evaluation of thermal insulation products | FR comments: The French Authorities would like to draw attention to the wording of prEN 13172:2007 concerning complaint procedures. If a product is non-compliant, a complaint is not generally lodged with the judicial authorities until attempts to settle a claim out of court have failed. The complaint procedure is a matter for the judicial authorities in application of the legislation and regulations in force, which take precedence over any contractual clauses, even if standardised and voluntarily agreed by all the contracting parties. As regards Annex F, which is described as being "informative", the penultimate paragraph of the foreword already states that: " .... Although the Annexes are informative in this standard, their use by the manufacturer will require that they assume a normative status. When an Annex is used the requirements in the Annex shall be followed, as given in the text." This could give the impression that manufacturers or users have no real protection and that application of the Standard does not give them any genuine rights. This undermines the credibility of the standards system and the French Authorities would like to see structural measures introduced with a view to preventing such situations from arising in future. |  |  |
| EN 14023. Bitumen and bituminous binders. Framework specification for polymer modified bitumens | Spain Harmonized part of EN 14023 does not cover all the technical requirements given in the regulations of the Spanish Roads Administration (General Technical Prescriptions for Roads and Bridge Construction, in force since 1999, and more specifically in its article 215 “modified bitumen”. The missing requirements for modified bitumen to be included into harmonized part of EN 14023 are: − Fraas breaking point − Storage stability − Elastic recovery These requirements are already included in general part of EN 14023, referred in table 2 as additional requirements and characteristics that have been considered useful for specifications. Besides, there is the NOTE 1, which explains: Each country will then have a particular selection of specifications, which, if regulated, are covered in table 1 and which if commonly used by industry, are covered in table 2. It is useful for each country to publish in a national guidance document for each application, their requirements for polymer modified bitumen from table 1 and table2. The appropriate class for each technical requirement or application is selected in turn and the selection of classes should be made from past experience of successful use, on a regulation basis, in order to avoid unworkable combinations. In our opinion it is not only useful to include some of the characteristics in a national guidance but necessary to have them included in regulations, and therefore it is necessary to have them included in harmonized part and in the CE marking assessment. It is not possible with actual EN 14023 to comply with Technical Spanish regulations, published in 1999 and in force since then. In these regulations it is based the experience of successful use on a regional basis. Further more, in our opinion, compliance with clauses of Annex ZA, does not guarantee satisfaction of the essential requirements, specially concerning with durability of works. 2 We propose that the three characteristics mentioned above, are transferred from table 2 (framework specifications for additional requirements and classes of polymer modified bitumen) to table 1 (framework specifications for essential requirements and classes of polymer modified bitumens) and which it is more important, that these characteristics are included in the harmonized part of EN 14023 in table ZA.1: − Technical characteristic 1: Fraass breaking point represents low temperature behaviour, due to the same reasons argued by Finland in the case of paving grade bitumens: it is necessary to cover durability of bituminous mixtures in cold climate. Spain has several areas at high altitude, with cold temperatures in winter. In addition, Fraass breaking point is mandatory in the Spanish polymer modified bitumen specifications (1999). − Technical characteristic 2: Storage stability. Difference in softening point plus difference in penetration. These characteristics must be considered covered by the mandate due to the durability, together with resistance to hardening. Unlike paving grade bitumen, the polymer modified bitumen could include in their formulations products with physical and/or chemical incompatibilities with bitumen. Therefore the storage stability is an essential characteristic to guarantee that the characteristics declared by the supplier do not suffer significant changes during the storage period. Storage stability is also a mandatory characteristic in the Spanish polymer modified bitumen specifications (1999). − Technical characteristic 3: Elastic recovery (25ºC & 10ºC). Some typical applications of polymer modified bitumens require a significant capacity to recover from high strain. For this reason, in many national specifications, Spanish included, elastic recovery is considered as a mandatory characteristic. If this characteristic were not included in the essential characteristics of table 1, then some polymer modified bitumen (such as those formulated with plastomer polymers) could comply with the specification but not with the performances required by clients in the intended use. This characteristic is related with resistance and durability of works and it is necessary for the assessment of the essential requirements 1 or 4. | 2009-06-17 Extract from CEN/TC 336 N300, RESOLUTION 2009/08 Subject: CEN/TC 336 – Anticipated revision of EN 14023:2005 The CEN/TC 336 Bituminous binders, - having considered the acceptance of an anticipated revision of EN 14023:2005 as stated in Resolution 2008/12 (CEN/TC 336 N 240) requested by AENOR (CEN/TC 336 N 226) - considering the formal proposal (draft EN 14023rev_(E)_v8 for TC336 Mtg_N263.pdf, associated to CEN/TC 336 N 252rev) elaborated by the CEN/TC 336/WG 1/TG 6 experts and accepted by the CEN/TC 336/WG 1; - considering the CEN/CENELEC Internal Regulations – Part 2, clause 11.2.3; - considering Resolutions BT 34/2002, BT 42/2003 and related document BT N 6962 concerning timeframes for the development of ENs; decides to launch a 3 month UAP (Unique Acceptance Procedure) ballot on: prEN 14023 Bitumen and bituminous binders – Specification framework for polymer modified bitumen. In accordance with the request by Spain, the CEN/TC 336 Bituminous binders underlines that the following characteristics are now included in the harmonised part of the standard: - Fraass breaking point, - elastic recovery. The CEN/TC 336 Bituminous binders accepts that homogeneity of PMBs is important, but homogeneity in the works is beyond the control of the binder suppliers and therefore the CEN/TC 336 decides to maintain the storage stability among the additional properties (Table 1C). |  |
| EN 14963 Roof coverings - Continuous rooflights of plastics with or without upstands - Classification, requirements and test methods | GERMANY: No characteristic values for the mechanical resistance of roof lights without upstands, are therefore applicable in interiors only. The design of construction works with respect to permanent loads (e.g. snow loads) for roof lights with upstand is not possible on the basis of the declared values given on the basis of this standard. The products are, therefore, applicable in snow-free areas only or if it is has been made sure that there is snow only for a short time. There are no provisions given for sampling and installation in the test room in the context of fire classification. |  |  |
| EN 15012 Plastics piping systems – Soil and waste discharge systems within the building structure -Performance characteristics for pipes, fittings and their joints | GERMANY: The possible materials are not finally defined, therefore an evaluation whether the tests foreseen are appropriate is impossible. The provisions for sampling and installation in the test room in the context of the fire classification are not representative. The provisions for the initial type-testing and for the factory production control are insufficient regarding checking the reaction to fire. prEN 15012 contains insufficient determinations concerning material restriction, technical requirements concerning reaction to fire as well as the verification of durability. When using waste pipes and fittings made of plastic within the building structure according to this standard the justified protection level existing in Germany will not be achieved. Due to the following substantial deficiencies the implementation of the standard in Germany in the present version can only be made in combination with special restrictions of use: - The scope of the draft standard is defined as follows: "This document specifies performance requirements for non-pressure plastics pipes, fittings and their joints intended for soil and waste applications: - inside the building (application area code "B"), - buried in ground within the building structure (application area code "BD") and with a diameter greater than or equal to 75 mm, and gives associated test methods for verification and evaluation of conformity with this document." Annex B of the draft refers to a set of product standards which includes “Specifications for pipes, fittings and the system” for the relevant materials. However, Annex ZA does not refer to Annex B; therefore, this list and hence the indications on the relevant materials and the constructive properties are not included in the harmonised part of the draft standard. The materials as well as the constructive properties on which the draft is based on are, therefore, not defined in any way. This means that the harmonised standard would also apply to such sewer pipes and fittings which are with respect to materials and to constructive properties not defined by other specifications (see Annex B). However, for both the material composition and the constructive design of the piping systems there are unlimited possibilities. Nevertheless, the draft standards foresees to verify their product properties according to the criteria described in the draft without having findings on that or could have findings at all whether these criteria are applicable to such products of undefined materials and with undefined constructive properties. This opening in the future harmonised standard would – from my point of view –violate the grouping provided for in the guidance paper for harmonised standards, since a completely undefined class would be formed because of this. This concerns in particular the durability. Though test methods are stated in the draft standard for the durability of sewage pipes and fittings; whether these are also enough for still unknown materials and constructions, is however extremely dubious. Testing the temperature cycling as verification for the durability is stated in section 4.4.1. But for the durability of sewer pipes and fittings verifications of the specific material properties, the physical and chemical properties as well as those of the treatment (e.g. requirements for the impact behaviour) are decisive. The specific requirements and verifications for unknown materials and constructions and the extent of the verifications necessary for that can only be defined and specified in the individual case. This is only possible in the context of an approval procedure. German representatives on CEN/TC 155 have urgently expressed themselves against the opening clauses in the draft standard. At least two delegations, from Portugal and Germany, had raised a similar case. This concerned a corresponding opening clause in EN 10138 for pre-stressing steels. Though it is understandable that on the part of the industry there is the request to ensure that also in the future all newly developed construction products will directly be covered by harmonized standards. But it faces the fact that with this approach maintaining the national safety and protection level cannot be guaranteed. Only by research and by experience, where relevant, it can be verified that certain known criteria are applicable to newly developed materials for example. - The stipulations of the standard for the determination and surveillance of the reaction to fire are not suitable to guarantee the necessary safety level in Germany. For the verification of the reaction to fire, reference is made in Annex A of the draft standard to the assembly and fixing of construction components in the test device according to EN 13823. The opinion of the responsible German authorities is that this reference is not practice-oriented. In the former European group of the "Fire Regulators" the German representative had expressed himself against this stipulation. The test procedure according to EN 13823 was prepared in order to determine the reaction to fire of basically even construction products. The treatment of some product families, e.g. of linear construction products (pipes, ventilation ducts, cables, etc.) can therefore require special rules, as they are stated in DIN EN 13823 section 1 "Notes". The determination of the class limits for the reaction to fire according to DIN EN 13501-1 in Germany is based on investigations on even construction products. The test set-up shown in Annex A makes a mass available substantially smaller compared with planar construction products. Therefore the test results cannot be adequately evaluated with the classifications limits given. The test set-up according to Annex A of the draft standard does not represent the built-in state either, as required in section 4.3.1.1 of the Interpretative Document "Safety in case of fire". Sewers are usually installed together with other sewers and/or pipe installations the reaction to fire of which affects each other. - The regulations in sections 6.2.2 "Initial type-testing" (Table 3) and 6.3.2 "Factory Production Control Requirements" (Table 4) contain insufficient stipulations for checking the reaction to fire. The manufacturing process of the moulding material has a considerable influence on the reaction to fire. Therefore the tests have to be performed on the final product. - Regarding the statements made in Annex ZA.3.1 on the shortened CE marking reference is made to the remarks attached as enclosure. The request is made to correct the insufficiencies presented: - to delete all opening clauses from the draft standard for the consideration of unknown materials and constructions. The draft standard should solely refer to the standards stated in Annex B; - to take into account the proposals made in the context of our cooperation for the verification of the reaction to fire. | 2009-06-17 Information awaited. The Commission had agreed to organize a meeting with the representatives of CEN/TC 155 and German and The Netherlands experts to look that the problems raised by the two Member States. TC 155 is awaiting the proposal of the meeting date. TC considers that ess. Characteristics are more than those defined in the mandate | TC to revise its reply to M131 taking into account the recent TC meeting (Paris 2010). Commission will ask Member States to confirm the ess. characteristics |
| EN 15013 and EN 15014 | NETHERLANDS: Documents PG 182 and SCC May 08 agenda item 13.2 | 2009-06-17 Information awaited. The Commission had agreed to organize a meeting with the representatives of CEN/TC 155 and German and The Netherlands experts to look that the problems raised by the two Member States. TC 155 is awaiting the proposal of the meeting date. On behalf of CEN/TC 155 we would like to respond to the VEWIN letter as follows. Around 1993, the CPD induced the start of standardization process for the hENs. Already in 1995, CEN/TC 155 took the principal decision to prepare cluster standards. The formal decision was taken in 1999. The cluster hEN approach was decided because of a number of reasons and was supported by the CEC representatives. During the years many discussions have taken place between the CEC, the CEN consultants and a number of experts from CEN/TC 155. The first answer to Mandate M/131 was submitted in September 2000. The observations of the Commission Services were received five months later. Further discussions took place in 2003 until final agreement was reached in October 2003 and confirmed in December 2003. During these years the draft standards were updated frequently to accommodate the evolving views of the Commission and better understanding. The CEN members had been informed on the developments through reports, circulation of the draft standards and through participation in the drafting committees. The drafts were circulated to the CEN members twice in 2001, once in 2003, twice in 2004, once in 2005, once in 2006 and once in 2007, i.e. eight times in total. A total of five times comments were requested during the years 2001 to 2007. VEWIN has withdrawn from the standardization process a number of years before the letter was written. Despite of many warnings to VEWIN with explanations of the importance and possible impact this standardization work might have, VEWIN kept well away from standardization. Only during the second vote, between 2007-03-22 and 2007-07-22, i.e. the 8th time the documents were available for comment or vote, VEWIN sent a copy of the letter in question to the secretariat on 2007-05-04 with the request to circulate it to the members. Also the Dutch authorities have requested the (Dutch) secretariat of CEN/TC 155 to circulate the letter before the deadline of the vote on the draft standards. Circulation of the letter was refused, firstly because this would be seen as an attempt of influencing the voting result by an organization that did not want to participate in standardization and secondly because at least a part of the argumentation had been refuted and could cause confusion. The letter was written without the involvement of the Dutch mirror committee. However, the tenor of the VEWIN objections has been discussed between VEWIN and the members of the mirror committee, but it is understood that the mirror committee could not support the letter. CEN/TC 155 discussed the VEWIN letter in its plenary meeting of November 2007. Under the agenda item "Concern regarding calls for tenders in the light of the PPD and CPD" the chairman explained why the document (see 155 N 3171) had been circulated. He confirmed that the issue shall be approached as a real problem if VEWIN sees a real problem. In this respect it should however be noted that none of the water companies of other European countries has expressed any of these concerns. In the meeting the Dutch delegation stated that there is communication between the Dutch manufacturers association and VEWIN and that at this stage no TC action was needed. However, VEWIN had meanwhile decided not to discuss its problems until the letter of complaint had been dealt with on CEC level. This position had surprised us, because it is felt that, whatever position the SCC will take, the concern of VEWIN must be taken away. Consequently discussions may have to take place anyway. The contents of the letter of VEWIN with its annexes gives the impression that VEWIN, as a purchaser calling for tenders under the PPD, is convinced that it may not require additional durability requirements that are considered necessary for purchasing products of the same quality as the quality of the products currently installed and are considered necessary for the Dutch situation. Consequently WEVIN would be forced to accept any CE marked products that are offered in the tender that should be accepted under the PPD. Furthermore is the arguing in direct conflict with answers given by the Dutch minister responsible for the building sector to questions in the Dutch parliament from the parliamentary committee for building etc in December 2007. The minister has answered recently. CEN/TC 155 understood from many discussions that the standards should be drafted such that the properties of the CE marked products are known through the associated information. This gives the required transparency in the market. Purchasers can then determine the product requirements on the basis of intended application, the (specific) conditions of use and any national regulation. Through these product requirements the purchaser can evaluate the information that accompanies the marketed products and make his choice. The standards of CEN/TC 155 are drafted in the light of the above understanding. | TC to revise its reply to M131 taking into account the recent TC meeting (Paris 2010). Commission will ask Member States to confirm the ess. characteristics |
| EN 15274 General purpose adhesives for structural assembly - Requirements and test methods | DE comments: The standard does not consider ER 2 contrary to the respective mandate. |  |  |
| EN 15275 Structural adhesives | DE comments: The standard does not consider ER 2 contrary to the respective mandate. |  |  |
| EN 15650 Ventilation for buildings – Duct mounted fire dampers | GERMANY: The standard comes under no mandate for product standards. CEN informs on the Internet that the standard will not be harmonized. Nevertheless, it contains an Annex ZA and in doing so refers to the horizontal mandate M117. | 2009-06-17 Answer of CEN/TC 156 to mandate M/109 being finalized. CEN/TC 156 position: CEN/TC 156 is still trying to secure a Mandate for EN 15650. If we do not get the Mandate by the time the document is ready for progression to Formal Vote, the Annex ZA will have to be removed; this will obviously slow down the process for the standard becoming harmonized. CMC position: CEN/TC 156 had wrongly made reference to mandate M/117. Having checked the situation more in detail, it believes that the product falls more within the scope of mandate M/109. | CEN/TC is expected to send a revised answer to mandate M109 |
| EN 15681 – 2 Glass in building – Basic alumino-silicate glass products – Part 2: Evaluation of conformity / Product standard | GERMANY: Meaningful documents which make an assessment of the product possible and, if necessary, the drafting of regulations for design and execution of construction works by using this product, are not available. Mechanical resistance and/or resistance against wind, snow and permanent loads must be indicated in “Pa”, not in “mm”. Furthermore, the standards refers to “generally accepted and/or conventional values” that may be used as basis for the declaration of the product’s performance with the CE marking. This is not appropriate as basis for setting up national regulations on design and execution of buildings.; DE reply to CEN comments (1/10/2009): The manufacturer should be able to provide the value of the characteristic bending strength as a product characteristic, which is irrespective of a design code. This is obligatory due to the product standard which allows "others" up to 8% as a magnitude of the proportions by mass of the principal constituents (section 4.1). The CE marking should ask for declaring the characteristic bending strength of 45·106 Pa instead of "Mechanical resistance and/or resistance against wind, snow and permanent loads in mm". The standard should provide for the responsibility for this value admitted by the glass manufacturer. He is responsible to determine this value according EN 1288. | 2009-06-17 Awaiting results of German examination of CEN position below. CEN/TC 129 position: It is impossible for a manufacturer to give the ‘Mechanical resistance’ of a glass pane in Pa for the following reasons: - A harmonised mechanical calculation method does not exist. The prEN13434 was to supply the method but when sent for enquiry received a large number of negative comments. Since that time TC 129 WG 8 has been working on revised parts that could be acceptable. - The load carrying capacity of a glass pane depends on many factors that the manufacturer would not necessarily be aware of. These factors are as follows: - Type of loading, i.e. wind, snow, self weight, or a combination of these loads. - Support condition of the glass pane, e.g. 4-edge, 3-edge, 2-edge, bolted. - Orientation of the glass plate, e.g. horizontal, vertical, sloping. - Whether or not the glass pane is being installed as single glazing, being incorporated into another glass product, e.g. laminated glass, insulating glass unit. The only value in the list of “generally accepted and/or conventional values’ that has been question is that for Characteristic bending strength. The working group, at the request of the DIN experts, are preparing an amendment to make this value one that is applicable for design. Additional comments provided by the TC Chairman. |  |
| EN 15682 – 2 Glass in building – Heat soaked thermally toughened alkaline earth silicate safety glass - Part 2: Evaluation of conformity / Product standard | GERMANY: Meaningful documents which make an assessment of the product possible and, if necessary, the drafting of regulations for design and execution of construction works by using this product, are not available. The provisions on the external surveillance and the retention time of the heat soaking do not correspond to an acceptable protection level. Mechanical resistance and resistance, respectively, against wind, snow and permanent loads must be indicated in "Pa", not in "mm". The failure pattern should also be tested on large panes. Furthermore, the standard refers to "generally accepted and/or conventional values" that may be used as basis for the declaration of the product's performance with the CE marking. This is not appropriate as basis for setting up national regulations on design and execution of buildings. DE reply to CEN comments (1/10/2009): The CE marking should ask for declaring the characteristic bending strength of 120·106 Pa and 75·106 Pa respectively instead of "Mechanical resistance and/or resistance against wind, snow and permanent loads in mm". The standard should provide for the responsibility for this value admitted by the glass manufacturer. He is responsible to determine this value according EN 1288. The provision of external surveillance and the differing retention time for the heat soaking in Germany is due to national experiences with problems of the heat soak process or the ovens. Those problems were detected by third independent parties with an independent control system. Heat soaked glass panes are applied as reliable products in areas where a glass failure is not acceptable. This means, a high control level is expected. According to our experience an amendment of mandate M135 for the heat-soaked thermally toughened soda lime silicate safety glass would be appropriate with regard to change the system of attestation of conformity to system 1+ (see the file annexed). The manufacturer should guarantee that the whole pattern is treated as required. This means, that the whole pattern, also the biggest, should have the typical glass structure after fracture. If the manufacturer would give a declaration for this, this would be enough. | 2009-06-17 Awaiting results of German examination of CEN position below. CEN/TC 129 position: The comment regarding ‘The provision of external surveillance and the retention time for the heat soaking do not corresponding to an acceptable protection level’ is a purely German view. The DiBT has required a third party certification, i.e. System of Attestation of Conformity – Level 1, be applied to EN 14179-2: Glass in building – Heat soaked thermally toughened soda lime silicate safety glass – Part 2: Evaluation of conformity/Product standard together with in increase in the retention time from 2 hours to 4 hours. No explanation of these changes has been given. The scientific evidence points to the heat soaking system contained with prEN 15682-2 and EN 14179-2 to be vastly superior to that existing in Germany before work on these standards commenced, The comment on ‘Mechanical resistance’ is covered above under EN 15681-2. The comment regarding ‘Failure pattern’ being tested on the largest panel has not been explained. The working group experts decided that the use of a set test specimen size for both ‘initial type testing’ and ‘product control under factory production control’ gave the manufacturer more consistency. The testing of the largest pane, i.e. the biggest that could be manufactured, will not give good process/product control. The comment on ‘Generally accepted values’ is covered above under EN 15681-2. Explicit values for ‘Characteristic bending strength’ and ‘resistance against sudden temperature changes and temperature differentials’ are given within the standard. Additional comments provided by the TC Chairman. | . |
| EN 15683 – 2 Glass in building – Thermally toughened soda lime silicate channel shaped safety glass - Part 2: Evaluation conformity / product standard | GERMANY: Meaningful documents which make an assessment of the product possible and, if necessary, the drafting of regulations for design and execution of construction works by using this product, are not available. Mechanical resistance and/or resistance against wind, snow and permanent loads must be indicated in "Pa", not in "mm". Furthermore, the standards refers to "generally accepted and/or conventional values" that may be used as basis for the declaration of the product's performance with the CE marking. This is not appropriate as basis for setting up national regulations on design and execution of buildings. DE reply to CEN comments (1/10/2009): The manufacturer should be able to provide the value of the characteristic bending strength as a product characteristic which is irrespective of a design code. The behaviour of those products is quite different to those of float glass, as the building elements with different dimensions are assessed, not only the material. | CEN/TC 129 position: It is impossible for a manufacturer to give the ‘Mechanical resistance’ of a glass pane in Pa for the following reasons: - A harmonised mechanical calculation method does not exist. The prEN13434 was to supply the method but when sent for enquiry received a large number of negative comments. Since that time TC 129 WG 8 has been working on revised parts that could be acceptable. - The load carrying capacity of a glass pane depends on many factors that the manufacturer would not necessarily be aware of. These factors are as follows: - Type of loading, i.e. wind, snow, self weight, or a combination of these loads. - Support condition of the glass pane, e.g. 4-edge, 3-edge, 2-edge, bolted. - Orientation of the glass plate, e.g. horizontal, vertical, sloping. - Whether or not the glass pane is being installed as single glazing, being incorporated into another glass product, e.g. laminated glass, insulating glass unit. The only value in the list of “generally accepted and/or conventional values’ that has been question is that for Characteristic bending strength – f g,k . The working group, at the request of the DIN experts, are preparing an amendment to make this value one that is applicable for design. Additional comments provided by the TC Chairman. |  |
| EN 15732 expanded-clay lightweight aggregates for lightweight fill and thermal insulation in civil engineering | FR comments: Standard EN 15732 on expanded-clay lightweight aggregates for lightweight fill and thermal insulation in civil engineering has been established under CEN TC 88. The French Authorities wonder whether essential requirement No 3 on hygiene, health and the environment has genuinely been taken into account in this Standard, since in the body of the text a paragraph headed "dangerous substances" refers the reader to Annex ZA1, which refers back to the original paragraph. Various solutions are possible. The French authorities propose the approach described in the following point. |  |  |