TECHNICAL QUERIES FOR CEN/TC – December 2012

QUERIES CONCERNING ALREADY CITED hENs

| EN TITLE | QUERIES | CEN / EC / MS POSITION | WAY FORWARD |
| --- | --- | --- | --- |
| EN 520 Gypsum plasterboards – Definitions, requirements and test methods | GERMANY: Concerning "Mechanical resistance and stability" information on characteristic values are missing. Instead of mean values the indication of characteristic values is required. Further German explanation: The standard contains test methods which lead to the calculation of mean values. Nevertheless, these mean values are not reasonable - especially in terms of the economically acceptable use of the products concerned - to be converted into characteristic values by being multiplied with national partial safety factors. Furthermore, the standard does not contain any characteristic value for bending, compression, tension and embedding strength which are essential according to the respective design codes. |  | Technical issue to be considered by the TC |
| EN 681-2 Elastomeric seals – Material requirements for pipe joint seals used in water and drainage applications – Part 2: Thermoplastic elastomers | GERMANY: For the permanent sealing effect by thermoplastic seals not only the deformation and relaxation behaviour under compressive load is decisive, but – depending on the construction – also under tensile stress. Increasingly there are thermoplastic seals available, the sealing effect of which is based on the tensile stress as far as the construction is concerned. These developments are not sufficiently covered in the standard. | CEN Position (2011-12-06): Technical issue to be dealt within CEN/TC 208 "Elastomeric seals for joints in pipework and pipelines" EC Position: These are specific technical issues which should not be seen as regulatory issues. | Technical issue to be considered by the TC |
| EN 845-1:2003+ A1:2008: Ties, tension straps, hangers and brackets standard | FINLAND: Standard included some serious deficiencies from the point of view of a regulator. The deficiencies are the following: - Clause 5.3: Characteristic load bearing capacity shall be given for those ancillary components (i.e. tension straps, hangers and brackets) which are acting independently. For example timber beam is designed based on characteristic load bearing capacity. That is why the bracket supporting the beam should also be designed based on characteristic load bearing capacity, not based on mean load bearing capacity. - Clause 5.3.4: The standard EN 845-1 is based only on testing. However load bearing capacity of slip ties (head restraint type) is declared based on calculation according “accepted engineering principles”. This not acceptable and these ties should be removed from the standard or test methods should be developed. - Clause 8.3: More precise FPC rules are needed. For example testing frequencies for FPC characteristics shall be specified. There is no notified body position paper concerning these products. - Table ZA.1: All the information given in the table 1 is related with the mandated characteristics. This shall be given in table ZA.1 as proxy characteristics. - Figure ZA.1: CE-marking example needs complete rewriting Note: Standard EN 845-1 is under review in CEN TC 125. New EN 845-1 will include improvements compared to the existing EN 845-1:2003 but it seems that the deficiencies presented above will not be solved. | CEN Position (2011-12-16): The Finnish queries have been taken into account and the draft will be sent to formal vote. Early in 2012. | Technical issue to be considered by the TC |
| EN 845-2:2003+A1;2008 Lintels | FINLAND: Standard includes a lot of serious deficiencies from the point of view of a regulator. The main deficiencies are the following: - General: The mandate M116 and table ZA.1 in the standard specify the lintels to support the loads over openings in masonry walls with a semi-structural role in the works. It is not specified what the semi-structural role actually means. In any case in Finland lintels are also used to support the loads over openings in masonry walls with a (normal) structural role in the works. Proposal: The mandate M116 shall be modified to cover lintels with a (normal) structural role in the works and a harmonised product standard shall be prepared for them. Scope of EN 845-2 shall clearly state that it covers lintels only for semi-structural use and an explanation is given what semi-structural role means. - Clause 5.3: Mechanical performance shall cover SLS examinations i.e. crack width (when relevant) and long term deflection. - Clause 5.3.2: The characteristic load bearing capacity for lintels shall be declared as characteristic value (confidence level 75 % and 5 % fractile). Principle of the EN 1990 shall be followed. - Clause 5.3.4: Determination method is just given for the short term deflection. However, the national requirement levels are given for long term deflection. Calculation methods have to be developed to determine the long term deflections of different kind of lintels. It is too expensive to use long term loading tests to determine long term deflection. - Clause 5.7.1: It is impossible to declare just “freeze/thaw resistant” or “not freeze/thaw resistant” since freeze/thaw resistance requirements vary in different Member States due to different climatic conditions. More specified verification method and declaration is needed. - Clause 8.3: More precise FPC rules are needed. For example testing frequencies for FPC characteristics shall be specified. There is no notified body position paper concerning lintels. - Table ZA.1: Separate tables ZA.1a, b and c are needed for single lintels (combined lintels), composite lintels and prefabricated parts of composite lintels. - Table ZA.1: All the information given in the tables 2 and 3 is related with the mandated characteristics. This shall be given in table ZA.1 as proxy characteristics. - Figure ZA.1: CE-marking example needs complete rewriting. Separate CE-marking examples are needed for single lintels (combined lintels), composite lintels. Note: Standard EN 845-2 is under review in CEN TC 125. New EN 845-2 will include improvements compared to the existing EN 845-2:2003 but it seems that the deficiencies presented above will not be solved. | CEN Position (2011-12-06): Standard being revised Enquiry closed: 2010-06-28 At the CEN/TC125 Plenary meeting which end on 15 October 2010, it discussed the queries from Finland. The revised EN 845-2 standard have been out to CEN Enquiry and CEN/TC125/WG3 will be holding a meeting in February 2011 to resolve the comments received including those from Finland. It is understood that Finland will be represented at that meeting and CEN/TC 125 will try to reach an acceptable solution that can be included in the drafts submitted for formal vote. | Technical issue to be considered by the TC |
| EN 845-3:2003+A1:2008 Ancillary components for masonry | FINLAND: Standard included some serious deficiencies from the point of view of a regulator. The deficiencies are the following: - Clause 5.3.3: In truss type welded meshwork cross-sectional area should be only area of the longitudinal wires. When given formula is used, the cross-sectional area is larger than total area of longitudinal wires and cross wire (area is determined from weight). - Clause 5.4.1.4: Shear load capacity of the welds shall be given as a characteristic load bearing capacity (confidence level 75 % and fractile 5 %). - Clause 5.5: Rules for determining anchorage and lap length from test results of the bond test should be presented in the standard. Declared values should be given with zero pre-compression. In addition the declared values with pre-compression may be given as complementary information. The Term “bond strength” is also misleading and it should be “bond force” (unit of strength is N/mm2 not N). The bond strength shall be given as a characteristic value (confidence level 75 % and fractile 5 %). - Clause 8.3: More precise FPC rules are needed. For example testing frequencies for FPC characteristics shall be specified. There is no notified body position paper concerning these products. - Table ZA.1: All the information given in the table 5 is related with the mandated characteristics. This shall be given in table ZA.1 as proxy characteristics (i.e. cross sectional area or wire size are not mentioned in table ZA.1) - Figure ZA.1: CE-marking example needs complete rewriting Note: Standard EN 845-3 is under review in CEN TC 125. New EN 845-3 will include improvements compared to the existing EN 845-3:2003+A1:2008 but it seems that the deficiencies presented above will not be solved. | CEN Position (2011-12-06): Standard being revised Enquiry closed: 2010-06-28 At the CEN/TC125 Plenary meeting which end on 15 October 2010, it discussed the queries from Finland. The revised EN 845-2 standard have been out to CEN Enquiry and CEN/TC125/WG3 will be holding a meeting in February 2011 to resolve the comments received including those from Finland. It is understood that Finland will be represented at that meeting and CEN/TC 125 will try to reach an acceptable solution that can be included in the drafts submitted for formal vote. | Technical issue to be considered by the TC |
| EN 998-1:2010 Rendering and plastering mortar | FINLAND: More precise FPC rules are needed. For example testing frequencies for FPC characteristics shall be specified. There is no notified body position paper concerning these products. | CEN Position (2011-12-06): Technical issues are the responsibility of CEN/TC 125 | Technical issue to be considered by the TC |
| EN 998-2:2003 Masonry mortar | FINLAND: Finland requests the modification of the standard. The characteristic bond strength (shear bond strength and flexural bond strength between mortar and masonry units) shall be included in the harmonised product standard. This characteristic bond strength is relevant for both the masonry units and mortar. It should be left to the manufacturers of masonry units and mortars to decide if the characteristic is declared in the CE-marking of masonry unit or in the CE-marking of masonry mortar. Note: Standard EN 998-2 is under review in CEN TC 125 but it seems that the above problem will not be solved | CEN Position (2011-12-06): Standard revised: 2010-09-15 The revised EN998-2 have successfully passed the UAP procedure and will be published. That completes the short term amendments which were agreed following the 5-year review. As part of longer term amendments CEN/TC125/WG2 will now address the outstanding issue concerning flexural bond strength. It was not included in original version of EN 998-2 because the test method EN1052-5 was not available at that time. | Technical issue to be considered by the TC |
| EN 1338 Concrete paving blocks – Requirements and test methods | GERMANY: The scope of this standard includes industrial areas, petrol stations and airport areas. These are areas which can be used for the handling of liquids hazardous to water like fuels or other chemicals. The standard contains no procedure to verify e.g. the chemical resistance of the products. Therefore, there should be a restriction in the scope of this standard so that the concrete paving blocks may not be used in facilities to deal with substances hazardous to water including service areas of petrol stations and service areas for the filling of airplanes and the tankers. |  | Technical issue to be considered by the TC |
| EN 1433 Drainage channels for vehicular and pedestrian areas – Classification, design and testing requirements, marking and evaluation of conformity | GERMANY: The foreword explains that the drainage channels are used to drain rain water at the most but that it is possible to use these channels also for the drainage of other liquids. The use categories are defined load dependent. Especially in use categories 5 and 6 the possibility occur to use the drainage channels according to this standard in areas which are used to deal with chemical liquids. However, the standard contains no procedure to proof e.g. chemical resistance. Therefore, there should be a restriction in the scope of this standard so that the drainage channels may not be used in facilities to deal with substances hazardous to water including service areas of petrol stations and service areas for the filling of airplanes and tankers. Furthermore, it is not possible to standardise the drainage channels with regard to such uses where they might come in contact with unknown media. |  |  |
| EN 1504-2 Products and systems for the protection and repair of concrete structures – Definitions, requirements, quality control and evaluation of conformity – Part 2: Surface protection systems for concrete | GERMANY: The standard does not describe a system but components. It is therefore, for the time being, left to national regulations to provide for indications on the systems, i.e. on the components to be used in combination. One of the requirements of this standard is the resistance of the sealing to chemicals including environmental influences and strong attacks of chemicals. This implies that surface protection systems according to the standard are suitable in e.g. chemical plants, but chemical plants are not part of the mandate M/128. In addition to that EN 13529 (the test standard for chemical resistance referred to in EN 1504-2) does not include all relevant media. At the moment we face a lot of developments with regard to bio fuels and other relevant media and to a lot of new materials so that the decisions relating to chemical resistance in EN 13529 are not in all cases correct. Therefore, there should be a restriction in the scope of this standard so that these surface protection products may not be used in construction works which are used for the handling of substances hazardous to water. | CEN Position (2011-12-01): Answer from CEN/TC 104/SC8: The standards listed are currently under revision by respective WGs and the queries made will be taken into during the revision process. Therefore, detailed anwsers to the queries will be formulated by working groups concerned as soon as possible. | Technical issue to be considered by the TC |
| EN 1504-4 Products and systems for the protection and repair of concrete structures – Definitions, requirements, quality control and evaluation of conformity – Part 4: Structural bonding | GERMANY: The standard does not describe a system but components. It is therefore, for the time being, left to national regulations to provide for indications on the systems, i.e. on the components to be used in combination. The standard contains no procedure to proof e.g. chemical resistance of the products. Therefore there should be a restriction in the scope of this standard so that the products and/or systems may not be used in facilities to deal with substances hazardous to water. | CEN Position (2011-12-01): Answer from CEN/TC 104/SC8: The standards listed are currently under revision by respective WGs and the queries made will be taken into during the revision process. Therefore, detailed anwsers to the queries will be formulated by working groups concerned as soon as possible. | Technical issue to be considered by the TC |
| EN 1504-5 Products and systems for the protection and repair of concrete structures – Definitions, requirements, quality control and evaluation of conformity – Part 5: Concrete injection | GERMANY: The standard does not describe a system but components. It is therefore, for the time being, left to national regulations to provide for indications on the systems, i.e. on the components to be used in combination. The standard contains no procedure to proof e.g. chemical resistance of the products. Therefore there should be a restriction in the scope of this standard so that the products and/or systems may not be used in facilities to deal with substances hazardous to water. | CEN Position (2011-12-01): Answer from CEN/TC 104/SC8: The standards listed are currently under revision by respective WGs and the queries made will be taken into during the revision process. Therefore, detailed anwsers to the queries will be formulated by working groups concerned as soon as possible. | Technical issue to be considered by the TC |
| EN 1916:2002 + AC:2006 Concrete pipes and fittings, unreinforced, steel fibre and reinforced | FINLAND: Finnish authorities and experts have found many deficiencies in EN 1916:2002 + AC:2006 Concrete pipes and fittings, unreinforced, steel fibre and reinforced. We ask the Commission to start actions so that these deficiencies can be corrected as soon as possible. EN 1916 is under revision in CEN TC 165 but unfortunately the latest draft does not include solutions on these problems. There seems to be similar deficiencies in EN 1917 Concrete manholes and inspection chambers, unreinforced, steel fibre and reinforced standard which shall be also corrected. The deficiencies found are the following: Foreword: 7th paragraph: It is not possible to open internal market for construction products if the situation as described in the paragraph exists in the harmonised product standard. "When the text of this European Standard was approved, complete agreement could not be achieved for all requirements in the existing national specifications of CEN members and so it includes only those requirements and associated test methods for which a consensus could be reached. Consensus was achieved on the requirements for quality control.” Standard has to be improved and the above text shall be deleted. CEN TC has the task to agree on the common European verification methods for all harmonised characteristics given in the mandate based on Member States regulations. It is not acceptable that the standard writes do not develop verification methods for all harmonised characteristics. According to the information we have received other national marks or approvals are required in addition to the CE-marking. These products are not necessary regulated by the Member States. Use of these products are under rules and conditions imposed by public bodies or private bodies acting as a public undertaking or acting as a public body on the basis of a monopoly. See article 6(1) of the CPD and also article 8(5) of the CPR. 1 Scope 1st paragraph: Nominal sizes of the pipes shall be increased up to 2000 mm. Table 1: Table 1 shall be modified as follows: TABLE could not be copied here Concrete: - Concrete and its constituents shall be specified according to EN 206-1. -> Add to 4.1 Materials and 4.2 Concrete to relevant clauses. Geometrical characteristics: - Dimensions and tolerances for internal dimensions of the pipe and for wall thickness shall be covered in this standard. Tolerances are related to structural characteristics. Tolerances can be given e.g. proportional to dimensional ranges. -> Add to 4.3.3 Geometrical characteristics to relevant clauses - Tolerances on the wall thickness shall be covered in this standard. Tolerances are related to structural characteristics. -> Add to 4.3.3 Geometrical characteristics to relevant clauses - Tolerances for the internal barrel length shall be covered in this standard. Tolerances are related to structural characteristics. Tolerances can be given e.g. proportional to dimensional ranges. -> Add to 4.3.3 Geometrical characteristics to relevant clauses - Deviation from straightness and from squareness of ends shall be covered in this standard. These characteristics are directly linked to watertightness and durability of the joints. Deviations are related to structural characteristics. -> Add to 4.3.3 Geometrical characteristics to relevant clauses Special requirements for steel fibre reinforced concrete pipes, reinforced concrete pies, jacking pipes and pipes with inlet: Rules how to define minimum concrete cover shall be added to this standard . -> Add to 5.2.2. Concrete cover - Limitations for spacing of the reinforcement as well as the relationship between internal and external reinforcing cages have to be added to this standard. -> Add to 5.2.1 Reinforcement - Tolerances on the external diameter of jacking pipe shall be covered in this standard. Tolerances are related to structural characteristics. Tolerances can be given e.g. proportional to dimensional ranges. -> Add to 5.3 Jacking pipes to relevant clauses. 4.1 Materials Table 3: Reference to EN 206-1 covers most of these items. Cement - Cement shall be according to EN 197-1. Aggregates - Aggregates shall be according to EN 12620. Mixing water - Mixing water shall be according to EN 1008 Additions There is no need to specify additions in this standard since requirements are given in EN 206-1. Admixtures Admixtures shall be according to EN 934-2. Steel fibres: - Steel fibres shall be according to EN 14889-1. Reinforcing steel: - Reinforcing steel shall be according to national standards valid in the place of use until EN 10080 is available as harmonised product standard. 4.2 Concrete See the comments after Table 1. 4.3.3 Geometrical characteristics See the comments after Table 1. 4.3.9 Durability Durability of the joint material shall be verified and declared in the CE-marking. 5.2.1 Reinforcement Limitations for spacing of the reinforcement as well as the relationship between internal and external reinforcing cages have to be added to this standard. 5.2.2 Concrete cover Rules how to define minimum concrete cover shall be added to this standard. 5.3 Jacking pipes Tolerances on the external diameter of jacking pipe shall be covered in this standard. Tolerances are related to structural characteristics. Tolerances can be given e.g. proportional to dimensional ranges. 7.2.4 Further testing of samples taken at the factory Note shall be modified as follows and made as normative text in clause 7.2.3 Factory production control, During factory production control the manufacturer is allowed to choose to carry out air or vacuum testing instead of hydrostatic testing for watertightness when correlation can be established between the reference test method (hydrostatic) and FPC test method (vacuum). 8 Marking Item e) shall be deleted. There is no need to mention notified body or any other third party in the normative text since the attestation of conformity system for pipes is system 4. Annex J Task for a product certification body This normative Annex shall be deleted. There is no need to mention notified body or any other third party in the normative text since the attestation of conformity system for pipes is system 4. Annex ZA Latest version of the model Annex ZA template developed by CEN consultants shall be followed. This includes the text concerning No Performance declared NPD-option which is now missing from the standard. Table ZA.1 ´New proxy characteristic ’Dimensional tolerances of the product’ shall be added to the list of essential characteristics. This characteristic is related with the strength characteristics. ZA.3 CE-marking The following information shall be added to the information accompanying the CE-marking: - Nominal size of the product - Relevant product dimensions and their tolerances - Information when the pipe includes integrated seal or seal is supplied separately - Dimensions and their tolerances relevant to joints - Concrete cover of the reinforcement Figure ZA.1 CE-marking examples given in Figure ZA.1 shall be updated since they do not follow the rules given in clause ZA.3. One example shall be given on the CE-marking when on the label or package including reference to the complete CE-marking given on the commercial documents. Another example shall be given on CE-marking information on the commercial document including identification of the product. This CE-marking example shall include declared values/classes for all characteristics listed in clause ZA.3. We ask that the Commission will take this item on the agenda of Queries group meeting and further on the agenda of PG and SCC meetings. |  | Technical issue to be considered by the TC |
| EN 1917 Concrete manholes and inspection chambers, unreinforced, steel fibre and reinforced | FINLAND: There seems to be similar deficiencies in EN 1917 Concrete manholes and inspection chambers, unreinforced, steel fibre and reinforced standard. |  | Technical issue to be considered by the TC |
| EN 10224 Non-alloy steel tubes and fittings for the conveyance of water and other aqueous liquids – Technical delivery conditions | GERMANY: Special tests for transport of water polluting liquids are not included in the standard. |  | Technical issue to be considered by the TC |
| EN 12101 – 3 Smoke and heat control systems – Part 3 | GERMANY: The functioning of the ventilators is only made sure if they are operated in an arrangement as they were tested. The classification of the fire resistance of the ventilators should consider the intended and tested position of the ventilators; the information should be given in the CE marking. Many test results obtained around Europe show that a motor tested in accordance with Annex D (test of the motor without the fan) do not pass the test together with the ventilator. Therefore, Annex D should be deleted. | CEN Position (2011-12-06): Technical issue to be dealt within CEN/TC 191 | Technical issue to be considered by the TC |
| EN 12101-6 Smoke and heat control systems – Part 6: Specification for pressure differential systems – kits | GERMANY: The standard includes only very little information on the product itself. The main body of the standard relates to the design and installation of the "kit". With this particular kit, CE-marking can only be done after it has been installed in a particular building. However, a product is required to be CE-marked before it is placed on the market. Therefore, the opinion of EC Services relating Table ZA.1 as given in PG 193 is supported: "The clauses referenced in the column headed "Requirement clauses in this standard" do not generally link to test methods and performance requirements against such methods, but in fact link to non-specific text or in some cases link to text which sets requirements but does not provide for a defined test method. Essentially a notified body would be unable to carry out initial type testing of samples for most of the characteristics listed in the table. In fact the standard appears to be totally written around the testing and assessment of installed systems, not the testing of samples. The standard does not provide for CE marking of the kit as such, but provides for some form of testing and acceptance of installed systems. For CE Marking purposes the standard would have to be completely rewritten." However, EN 12101-6 is still on the list of the harmonised standards, but no CE-certificates can be issued. | CEN Position (2011-12-06): Technical issue to be dealt within CEN/TC 191. CEN/TC 191 has agreed to draft a specific part to deal with the design aspects. | Technical issue to be considered by the TC |
| EN 12285-2 Workshop fabricated steel tanks – Part 2: Horizontal cylindrical single skin and double skin tanks for the above ground storage of flammable and nonflammable water polluting liquids | GERMANY: The scope of EN 12285-2 exceeds the scope of the mandate. EN 12285-2 designates in the scope all water polluting liquids up to the maximum density of 1,9 kg/l while the mandate covers only densities to 1.0 kg/l. German explanation and answer to CEN position: M131 is covering liquids for heating or cooling of buildings, or water. Such liquids have a density of 1.0 or less. | CEN Position (2011-12-06): Technical issue to be dealt within CEN/TC 265. TC265-M/131 There is no scope limitation in the mandate | Technical issue to be considered by the TC |
| EN 12620:2002/A1 Aggregates for concrete | GERMANY: The range of application of the standard is defined wide enough so that also recycling products can come under it. But requirements concerning environmental compatibility are not defined. CEN/TC 154 will catch up on this with the next revision. Besides, until now – for lack of harmonized test methods – the property "alkali-silica reactivity" has not been harmonized yet. There is no European agreement on an ASR test. CEN/TC 154 has a combined task group with TC51 and TC104 working towards a unified standard for minimising ASR risk in concrete. Current activity involves determination of available alkalis in cement, aggregates and additives. | CEN: Formal requirements for recycled aggregate were incorporated by amendment about two years ago but they have been in the scope from the original standards. In the current five year review, CEN/TC 154 have done a lot to clarify much more precisely what is in and what is out of scope, particularly regarding secondary aggregate sources. I'm not sure what is meant by 'environmental compatibility'. If it means regulated dangerous substances, CEN/TC 154 has indicated it shall include in a future revision, in accordance with the Mandate amendment. The position on alkali silica reactivity is unchanged from the original standards where CEN/TC 154 agreed to defer this to local requirements at the place of use. There is no European agreement on an ASR test. CEN/TC 154 has a combined task group with TC51 and TC104 working towards a unified standard for minimising ASR risk in concrete. Current activity involves determination of available alkalis in cement, aggregates and additives. | Technical issue to be considered by the TC |
| EN 12859 Gypsum blocks - Definitions, requirements and test methods | GERMANY: Concerning "Load bearing capacity" information on characteristic values are missing. Instead of mean values the indication of characteristic values is required. Further German explanation: The standard contains test methods which lead to the calculation of mean values. Nevertheless, these mean values are not reasonable - especially in terms of the economically acceptable use of the products concerned - to be converted into characteristic values by being multiplied with national partial safety factors. Furthermore, the standard does not contain any characteristic value for bending, compression, tension and embedding strength which are essential according to the respective design codes. |  | Technical issue to be considered by the TC |
| EN 13108-1 to 7 Bituminous mixtures | SPAIN: Deficiencies have now also been found in a series of harmonised standards, EN 13108 Parts 1 to 7 dealing with bituminous mixtures. Their references have been published in the OJEU and their period of coexistence ends in March 2008. In this case the deficiencies relate to margins of tolerances for contents of soluble binder and for grading of aggregates. Such deficiencies are found when using Parts 20, regarding Type Testing, and 21, regarding Factory Production Control, to which all first seven parts make reference for evaluation of conformity and therefore of compulsory application for CE marking. Details are provided in the attached document which, as the previous one, was received from Directorate General for Roads. The reason for submitting this new query is once again incompatibility with the national regulatory bill, the same as in the previous query, in force since 1999. A copy of relevant pages of I this bill are included in the attached document and related paragraphs are shaded in colour. Translation of those paragraphs will be provided if requested. This regulation was the subject of a notification under 98/34/EC directive with reference number 1999/340/E, and the complete text is available in English, French and German in TRIS. | Message from ES authorities on 2011-02-02: In relation to the query on EN 13108-1 to 7 Bituminous mixtures, this group of standards begin now a revision process in which, the CEN/TC227/WG1 has shown interest on discussing and trying to solve the queries presented by Spain. In this situation, we hope that the comments will be included in the future works of the Technical Committee, so we should wait and follow the development of the new version of the EN 13108 package. | Technical issue to be considered by the TC |
|  | Reaction from ES on 03/09/2009 by e-mail: Regarding the query of Spain on the European harmonized standards (series EN 13108. Bituminous mixtures) it is necessary to say: Background - In October, 2007, the Ministerio de Fomento sent a query to the SCC on the issue of the deficiencies discovered by the Spanish Directorate General for Roads in harmonised standards related with bituminous mixtures (series EN 13108) asking to be included under point 6 of the Agenda of the SCC Preparatory Group meeting held in October 8, 2007. - In November, 2007, the same document was sent again in order to be taken into account in the 66th meeting of the SCC of December, 2007. - On December 23, 2007, CEN, having been informed by the SCC of these deficiencies, released a report promising to discuss the same ones in the CEN/TC227/WG1 meeting of April 17, 2008. - In the CEN/TC227/WG1 meeting of April 17, 2008 in Reykjavik, the Spanish representative presented again the position of Spain, indicating that it had not been sufficiently understood, answering to the above mentioned report. In this intervention, he mentioned that Spain could agree with the part concerning tolerances but that DG Roads maintained its position on the part concerning the analysis of sensibility. Such observations were not included in the minutes of the meeting. - In July, 2008, a letter was sent to the SCC to which a report of Directorate General for Roads justifying the position of Spain in the same terms as summarized in the previous point is attached. - In the CEN/TC 227/WG1 meeting of October 27-28 in Zagreb, the Spanish representative requested the modification of the minutes in order to include the observations of Spain. - Finally, in the 68th meeting of the SCC of November, 2008, the Spanish representative raised again the query of Spain with regard to the series of harmonized standards EN 13108 . The above mentioned request was not included in the minutes of the meeting. In the 69th meeting of the SCC of June, 2009, the Spanish representative requested that the minutes of the previous meeting be corrected in its point 12 in order that the query of Spain is included. Conclusion The technical specifications of the Spanish roads regulation, in force since the year 2004 by means of the ministerial Order FOM/891/2004, of March 1, and of obligatory fulfilment in Spain, were not taken into account in the drafts of the harmonized standards. This regulation was the subject of a notification in conformity with the 98/34/EC directive, being the complete text available in English, French and German in TRIS as dossier 2003/102/E. As for the comment from CEN/TC227/WG1 reminding that AENOR (Spanish NSB in CEN) did not rise observations in the formal vote process of prEn 13108-20 and prEN 13108-21 standards, it is necessary to say that AENOR develops its activity in the private area, whereas the ministerial Order FOM/891/2004, of March 1, concerns the Spanish legislation and is approved by the Government. Since the Government of Spain had news of the content of the series of harmonized standards EN 13108, it has been reporting, both to the SCC and to CEN the existence of the national regulation that since the year 2004 has been establishing the mentioned technical specifications, without, up to the moment, being taken into account. We once more insist in the need to modify the series of harmonized standards EN 13108 in order to allow the fulfilment of the ministerial Order FOM/891/2004 just as it has been reported both in the SCC and in the CEN, through TC 227/WG1. Attached pleased find the report of of Directorate General for Roads justifying the position of Spain about deficiencies discovered in harmonised ENs 13108. Bituminous mixtures. Material specifications. Same report was previously sent 17/07/08. -------------------------------------------------------------------------------------- AUSTRIA on EN 13108-1: According to the Commission Decision there are four Systems of Attestation of conformity (AoC) applicable to the product, i.e. AoC 1, 2+, 3 and 4 which is correctly reflected in table ZA.2. But there are only two tables ZA.3. Table “a” for AoC 2+ and table “b” for AoC 1. Our observations regarding these tables are: − Corresponding tables for AoC 3 and 4 are missing. There are no tables which clarifies the tasks for the manufacturer and the approved body for AoC 3 and 4. − In table ZA.3a within “tasks of the manufacturer” testing by a “notified laboratory” is requested. This is a contradiction, as testing by a notified laboratory is the task of the notified body and not of the manufacturer. | TC expected to correct the EN |  |
| EN 13162 “Thermal insulation products for buildings - Factory made mineral wool (MW) products – Specification” to EN 13171 | FINLAND: Comments on harmonised standards for thermal insulation products i.e. EN 13162…EN 13171 Note: Especially comments are prepared for EN 13162 Thermal insulation products for buildings – Factory made mineral wool (MW) products – Specification 1. Solutions needed in the short term 1.1 Declared values for thermal resistance and thermal conductivity The rules how to determine declared values of thermal resistance and thermal conductivity should be clarified. In the Annex A it has been written correctly that it is the responsibility of the manufacturer to determine the declared values of thermal resistance and thermal conductivity. However, clause 4.2.1 and also Annex D give an other interpretation. The declared value of thermal conductivity shall not be the calculated value λ 90/90 after rounding upwards to the nearest 0,001 W/(mK) using the step of 0,001 W/(m K) from ITT tests as it can be now understood from the standards. The declared value of thermal insulation resistance shall not be the calculated value R 90/90 after rounded downwards to the nearest 0,05 m2 K/W from ITT tests as it can be now understood from the standards. The manufacturer has to determine the declared values based on evaluation of ITT test results. The declared values must be on safe side compared to the calculated λ 90/90 or R 90/90 values from ITT population of samples. Then in continuous factory production control the manufacturer has to show that the calculated λ 90/90 or R 90/90 value from FPC population are in the limit of the declared value (on the "safe" side). There should not normally be a need to declare other new declared values when mean values and variations of results are regularly calculated for FPC population according to Annex A. 1.2 Influence of air flow resistance (convection) to the thermal resistance/conductivity (only relevant for EN 13162) It is a physical fact that convection will increase considerably the thermal resistance and decrease considerably thermal conductivity of thick insulation layers in the building envelope. Nowadays it is not possible to take this phenomenon into account in design since CE-marking of mineral wool does not normally include information on its convection behaviour i.e. its air flow resistance. This characteristic is only declared in the CE-marking if product is used for sound insulation applications. That is why it is necessary to add into Table ZA.1 in EN 13162 a third proxy characteristic ‘air flow resistance’ under the mandated characteristic ‘Thermal resistance’. In this way it is possible in national rules (for the determination of design thermal resistance/conductivity from declared values) to take convection in account by using only CE-marking information as input values of the calculation. There is no need to modify the mandate M102. TC 88 answer to the mandate just needs updating. 2. Solutions needed in the long term 2.1 Harmonised product standards for thermal insulation products taking into account the intended end use of the product Harmonised product standards for thermal insulation products have been prepared to cover all kind of end uses. Normally the manufacturers just declare in the CE-marking that their products are intended of all applications in the building. Unfortunately this means that the harmonised product standards for thermal insulation products do not take into account the specific regulatory needs of different end use applications of thermal insulation products. For example thermal insulation may be fixed on the roof by using mechanical fixings. Existing harmonised product standards do not include any characteristic which could give information if the product is applicable to be used with the mechanical fixing and which kind of forces can be transferred. Harmonised product standards should be further developed to handle the different end use applications of thermal insulation products i.e. separate Tables ZA.1 for different end-use applications are needed to the harmonised product standards. Note: For many other construction products (See e.g. EN 12602 ‘Prefabricated reinforced components of autoclaved aerated concrete’) this kind of approach is already in use. TC 351 has made a conclusion that before dangerous substances can be covered in harmonised product standards the intended use of the product has to be specified more accurately than nowadays in the CE-marking. 2.2 Determination of design thermal resistance or conductivity Declared thermal resistance/conductivity values are given in the CE-marking. These declared values cannot be used in the design of structures since they do not take into account the practical and long term conditions of thermal insulation products in different end uses. Design thermal resistance/conductivity values are used in the calculation of energy efficiency of buildings. Design thermal resistance/conductivity values are nowadays determined from declared thermal resistance/conductivity values using national calculation methods. It would be beneficial for the internal market of construction products if European guidance (e.g. EN-standard) is developed to help the Member States to give coherent rules for the determination of design values from declared values for different insulation materials. |  | Technical issue to be considered by the TC |
| EN 13341 Thermoplastics static tanks for above ground storage of domestic heating oils, kerosene and diesel fuels – Blow moulded polyethylene, rotationally moulded polyethylene and polyamide 6 by anionic polymerization tanks – Requirements and test methods | GERMANY: EN 13341 regulates containers in a way which doesn't make it possible to maintain the German level of safety (e.g. with regard to lockable openings underneath the maximum filling level), or for which special requirements are valid (filling with kerosene - flash point under 55°C; inspection opening for capacity > 2000 l). For effects from earthquakes and for the reaction to fire behaviour the standard does not make any declaration. GERMANY: EN 13341 comprises provisions for containers in a way which doesn't make it possible to maintain the German level of safety (e.g. with regard to lockable openings underneath the maximum filling level), or for which special requirements are valid (filling with kerosene - flash point under 55°C; inspection opening for capacity > 2000 l). With regard to the verification of the time where the tank is still able to hold the fuel during a fire (leak tightness during 30 minutes of fire impact - but it is not the same as fire resistance) we suggest to integrate the test which is already described in prEN15724:2007. | CEN Position (2011-12-06): EN 13341 it does not regulate anything. Moreover, reaction to fire is considered while the resistance to fire was indicated as not being relevant in the original answer to M/131 prepared by TC 266. When they revised their answer, the justifications requested by EC regarding the excluded essential characteristics have been given. Specifically, regarding resistance to fire, the CEN/TC 266 experts are not aware of the existence of any regulation in Member States affecting the concerned products. When the document was addressed to EC for acceptance, the attention of the Commission was drawn up on their proposed request to amend the mandate in this respect. Earthquake does not originate any specific essential characteristic in the mandate. Therefore, in the lack of a mandate amendment, it should be considered as a voluntary characteristic that can be included in the standard it there is a consensus of the experts. The standard is not yet finalized | Technical issue to be considered by the TC |
| EN 13492 Geosynthetic barriers – Characteristics required for use in the construction of liquid waste disposal sites, transfer stations or secondary containment | GERMANY: From the technical point of view the standard is not suited for geosynthetic barriers for use in facilities to deal with liquids hazardous to water, because the main important characteristic, chemical resistance to the liquids stored in the facilities, is not and can not be covered by this standard. It is necessary to verify for each geosynthetic barrier the chemical resistance to all media which could get in contact with the geosynthetic barrier. Each material used for geosynthetic barriers is only resistant to certain media. The possible variations of product materials and media can not be covered by a standard. From the legal point of view the standard could not cover geosynthetic barriers for the use in facilities to deal with liquids hazardous to water, because this application field is not included in the Mandate M 107. Therefore, there should be a restriction in the scope of this standard so that the geosynthetic barriers should not be used in facilities to deal with liquids hazardous to water. The product standard does not consider ER 2 "Safety in case of fire". Germany has regulations requesting the determination of the reaction to fire characteristic of that product. |  |  |
| EN 13813 Screed material and floor screeds – Screed materials – Properties and requirements | GERMANY: From the technical point of view the standard is not suited for screed materials for use in facilities to deal with liquids hazardous to water. The test procedure in the standard is not suitable for all screed materials. The screed materials have to be chemical resistant and liquid tight to chemicals. Due to EN 13318 which is referred to in EN 13813, screed materials can be: e.g. polymer modified cementitious screed or cementitious screed which is not liquid tight and has to be tested using another test procedure. In addition to that the referenced test standard EN 13529 does not cover all relevant media. At the moment we face a lot of changes concerning bio fuels and other relevant media and a lot of new materials so that the decisions relating to chemical resistance in EN 13529 are not in all cases correct. Therefore, there should be a restriction in the scope of this standard so that the screed materials may not be used in facilities to deal with liquids hazardous to water. |  | Technical issue to be considered by the TC |
| EN 13915 Prefabricated gypsum plasterboard panels with a cellular paperboard core - Definitions, requirements and test methods | GERMANY: Concerning "load bearing capacity" information on characteristic values are missing. Instead of mean values the indication of characteristic values is required. Further German explanation: The standard contains test methods which lead to the calculation of mean values. Nevertheless, these mean values are not reasonable - especially in terms of the economically acceptable use of the products concerned - to be converted into characteristic values by being multiplied with national partial safety factors. Furthermore, the standard does not contain any characteristic value for bending, compression, tension and embedding strength which are essential according to the respective design codes. |  | Technical issue to be considered by the TC |
| EN 13950 Gypsum plasterboard thermal/acoustic insulation composite panels - Definitions, requirements and test methods | GERMANY: Concerning "Mechanical resistance and stability" information on characteristic values are missing. Instead of mean values the indication of characteristic values is required. Further German explanation: The standard contains test methods which lead to the calculation of mean values. Nevertheless, these mean values are not reasonable - especially in terms of the economically acceptable use of the products concerned - to be converted into characteristic values by being multiplied with national partial safety factors. Furthermore, the standard does not contain any characteristic value for bending, compression, tension and embedding strength which are essential according to the respective design codes. |  | Technical issue to be considered by the TC |
| EN 14064-1 “Thermal insulation products for buildings – In-situ formed loose-fill mineral wool (MW) products – Part 1: Specification for the loose-fill products before installation | GERMANY: The thermal conductivity should be declared as a limit value. Each single measured value of thermal conductivity shall not exceed the declared value. This declared value shall be determined within the ITT by a notified body only. This procedure would correspond to the task for the notified body in AoC System 3 as laid down in Annex ZA of the harmonized standard. In contrast to that the current Annex A of the standard which is referred to indirectly in Annex ZA says that only the manufacturer is responsible to determine the declared value (based on internal or external measurements). Annex A should be changed such that it will be clear that the declared value is to be determined based on measurements performed by a notified body only. In our opinion it is not necessary to use 10 or more measurement results. We propose to include at least 4 measurements. Based on these measurement results the declared value of thermal conductivity shall be laid down such that no measured value is higher than the declared value. It is up to the manufacturer to decide about the difference between the declared value and the worst measured value as he deems to be appropriate. But the declared value shall be kept in every case – that would also be a clear limit for the market surveillance which is missing at the moment. A product with a higher value of thermal conductivity than the declared value is then not in conformity with the declaration. Furthermore it would be necessary to have the thermal conductivity controlled by a notified body (System 1+). This would require a change of the mandate. The above proposal applies analogously to thermal resistance. The provisions concerning the settlement are not sufficient: For lofts: The field studies are not described. Basically, there are doubts that field studies are adequate as (sole) tests in order to determine generally accepted specifications. Only defined laboratory tests should be performed. The test according to Annex K does not include the determination of settlement due to vibration. Walls, masonry walls and frame constructions: Any test of settlement is missing. EN 14064-1 only includes the short term water absorption. For certain applications (e. g. core insulation of masonry walls) the long term water absorption is relevant too. In Germany requirements exist to verify the behaviour of products in respect of continuous glowing combustion in the case of fire. In the case of not considering this behaviour, an additional national assessment e.g. on the basis of national procedures would have to be required. The provisions concerning reaction to fire are not sufficient for a classification. For mounting and fixing provisions EN 14064-1 includes a reference to EN 15715. But this standard does not include appropriate provisions for this kind of products. |  |  |
| - EN 14080:2005 Timber structures – Glued laminated timber – Requirements | FINLAND: EN 14080 has not drafted according to Guidance Paper L and Guidance Paper K. The 3 Methods of GP L has not been mentioned. Standard includes three CE-marking examples. Figure ZA.1 and ZA.2 present CE-marking information appearing on the accompanying commercial documentation. Figure ZA.3 present CE-marking information to be shown on the product. We can interpret that Figure ZA.1 and ZA.2 are based on the idea of Method 1 of GP L. Unfortunately geometrical data is missing. Methods 2 and 3a) and 3b) are missing. Method 1 means that products have been put on the market without knowing end use applications. However, glue laminated timber products are usually designed to a specific construction works as beams and columns. Methods 3a) and 3b) are absolutely needed. Method 3b) can be probably used from the second semester of 2007 when EN Eurocodes with National Annexes have been adopted in use at least in some Member States. It is totally unsatisfactory to have a harmonised product standard for structural products without having possibilities to use all those business models recognized by GP L which are in use in Member States. From regulators point of view it is impossible to demand that one product has to use CE-marking and the other does not depending on which business model will be used. If the product is under the scope of the standard all applicable business models shall be allowed for the manufacturer. That was one of the targets of Guidance Paper L. Detailed remarks Clause Z.2 The standard refers to other standards e.g. EN 386 ‘Glued laminated timber - Performance requirements and minimum production requirements’ (published 2001) and EN 387 ‘Glued laminated timber - Large finger joints - Performance and minimum production requirements’ (published 2001). EN 386 includes its own factory production control, organization of factory production control and inspection and testing rules. EN 387 includes its own factory production control, organization of factory production control, inspection and testing rules and also Annex A ‘The task of the third party certification body’. Attestation of conformity decision is level 1 for glued laminated timber products. FPC rules in the harmonised product standard and in standards it is referring make understanding of the FPC rules for the CE-marking confusing and very difficult to understand. Clause Z.2.2.1, third paragraph Recognized glue-testing institute is mentioned. The CPD does not recognize this kind of institute. |  |  |
| EN 14081-1:2005 Timber structures – Strength graded structural timber with rectangular cross section – Part 1 : General Requirements | AUSTRIA / BELGIUM / GERMANY: Very expensive CE marking | CEN Position (2011-12-06): EN 1080:2005 : this standard is under revision (WI 00124133) , CEN enquiry ends on mid june 2011 and WG3 is dealing with the comments. Fire resistance is in clause 6.5 and dimensional stability in clause 6.8 and 6.9.2. Both characteristics are mentioned in table ZA1 in clause ZA.1 | Technical issue to be considered by the TC |
| EN 14179-2 Glass in building - Heat soaked thermally toughened soda lime silicate safety glass - Part 2: Evaluation of conformity/Product standard | GERMANY: The attestation of conformity system has to be amended by implementing provisions for an external surveillance, in order to reach a level of protection as given on the German national level. The fragmentation should also be tested on large panes (see EN 1863-2). | CEN Position (2011-12-06): Changing the system of attestation of conformity is the responsibility of the Commission and SCC. Why Germany has made this comment is unknown as they have not accepted the standard processing conditions but have increase the ‘holding time’ for their own version | Technical issue to be considered by the TC |
| EN 14188-1 Joint fillers and sealants – Part 1: Specifications for hot applied sealants | GERMANY: The test procedure includes a 24 hour test for chemical resistance against fuel. This is not sufficient for the use of these sealants e.g. in the service area of petrol stations. Therefore, there should be a restriction in the scope of these standards so that the sealants may not be used in facilities to deal with substances hazardous to water. |  | Technical issue to be solved at TC level. |
| EN 14188-2 Joint fillers and sealants – Part 2: Specifications for cold applied sealants | GERMANY: The test procedure includes a 24 hour test for chemical resistance against fuel. This is not sufficient for the use of these sealants e.g. in the service area of petrol stations. Therefore, there should be a restriction in the scope of these standards so that the sealants may not be used in facilities to deal with substances hazardous to water. |  | Technical issue to be solved at TC level |
| EN 14188-3 Joint fillers and sealants – Part 3: Specifications for preformed joint seals | GERMANY: The standard contains no procedure to verify e.g. chemical resistance of the products. In Annex ZA.1 the use of these preformed joint seals in service areas for the filling of airplanes and tankers is mentioned. This application has to be deleted. |  | Technical issue to be considered by the TC |
| EN 14190:2005 Gypsum plasterboard products from reprocessing – Definitions, requirements and test methods | EC services: The footnote to Table ZA.2 refers to Commission Decision 2003/43/EC which delas only with wood based products. The correct reference is Commission Decision 95/467/EC, which foresees AoC systems 1/3/4 for reaction to fire. |  | Technical issue to be considered by the TC |
| EN 14449 Glass in building – Laminated glass and laminated safety glass – Evaluation of conformity/Product standard | GERMANY: For laminated safety glass the properties of the interlayer as defined in the standard are not sufficient. For laminated glass and laminated safety glass according to the standard, sheets of plastic are allowed as glazing sheet material. This should be excluded since it would cause the necessity of a lot of further assessments with regard e.g. to the reaction to fire behaviour, to health protection, environmental influences, durability. Therefore, plastic glazing sheet material should be dealt with separately. German answer to CEN position: The interlayer shall be covered by glass sheets. With only testing acc EN 12600 at one temperature the interlayer is not sufficiently defined. A shear test or additional specifications for the material shall be requested. Further German explanation: In Germany the interlayer for laminated safety glass has to be defined. For laminated safety glass with other interlayer than such made of polyvinyl butyral (PVB) verifications are required by testing: A cracked pane has to pass a test to prove the remaining load bearing capacity whereas for certain uses e.g. this cracked pane loaded by 0,5 KN/m2 is not allowed to fail totally for 24 hours. Actually, within a German research project the characteristics of certain interlayers and their respective remaining load bearing capacity are being examined. The results are expected within 2012. | CEN Position (2011-12-06): Answer from CEN/TC 129: The standard covers all types of laminated glass/laminated glass. The type of interlayer does not need to be prescriptive, I,e, pvb as in Germany, A laminated safety glass is defined by its performance under EN 12600. The incorporation of plastics glazing sheet materials in laminated glass is important as it gives high performance security glazings with lower weight than all glass compositions | Technical issue to be considered by the TC |
| EN 14785 "Residential space heating appliances fired by wood pellets - Requirements and test methods" | GERMANY: The scope of EN 14785 should be modified so that the fireplaces with automatic loading facilities that are ready for connexion and that have a fan will be covered in this standard only. There are no experiences related to the other fireplaces. The risk to gas and dust explosions exists in particular in the case of fireplaces operated with natural delivery pressure. Therefore, for these fireplaces experiences must be gained necessarily before they can be covered by a standard. In the meantime the national application rules must be based on a case-by-case basis. |  | Technical issue to be considered by the TC |
| EN 15283-1 Gypsum boards with fibrous reinforcement - Definitions, requirements and test methods - Part 1: Gypsum boards with mat reinforcement | GERMANY: Concerning "Mechanical resistance and stability" information on characteristic values are missing. Instead of mean values the indication of characteristic values is required. |  | Technical issue to be considered by the TC |
| EN 15283-2 "Gypsum boards with fibrous reinforcement - Definitions, requirements and test methods - Part 2: Gypsum fibre boards" | GERMANY: Concerning the corner stones for FPC the requirements with regard to the necessary assessment within the framework of the surveillance as well as the frequency of the action required should be included in the standard. Furthermore, the standard contains test methods which lead to the calculation of mean values. Nevertheless, these mean values are not reasonable - especially in terms of the economically acceptable use of the products concerned - to be converted into characteristic values by being multiplied with national partial safety factors. Furthermore, the standard does not contain any characteristic value for bending, compression, tension and embedding strength which are essential according to the respective design codes. |  | Technical issue to be considered by the TC |
| EN 15285 Agglomerated stone - Modular tiles for flooring and stairs (internal and external) | GERMANY: The standard contains a procedure to verify the chemical resistance of the products. The criteria for the assessment of the chemical resistance do not meet the criteria for the use of these stones in facilities to deal with substances hazardous to water. Therefore, there should be a restriction in the scope of this standard so that the products for modular tiles may not be used in facilities to deal with substances hazardous to water. | CEN Position (2011-12-06): The test method was taken by the ASTM C-650 for testing ceramic tile that are to be used for food counters, lavatories, and similar residential, medical, and commercial installations, where they may come in contact with food, chemical, and waste substances and for tile in areas where they may be exposed to contact with strong cleaning agents. The specification of hydrochloric acid solution andpotassium hydroxide solution as normal testing fluids, and the length of exposure time and temperature are based on experimental laboratory work and interlaboratory tests, where it was indicated that resistance to these two substances probably assures resistance also to any other acidic or alkaline substance coming in contact with tile, except hydrofluoric acid. This standard does not purport to address all of the safety concerns, if any, associated with its use. It is the responsibility of the user of this standard to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to use. | Technical issue to be considered by the TC |
| EN 15824:2009 - Specification for external renders and internal plasters based on organic binders | AT comments: In table ZA.3.2 within “tasks of the manufacturer” testing by a “notified laboratory” is requested. This is a contradiction, as testing by a notified laboratory is the task of the notified body and not of the manufacturer. |  | Technical issue to be considered by the TC |

QUERIES CONCERNING CANDIDATE hENs

| EN TITLE | COMMENTS | CEN POSITION | WAY FORWARD |
| --- | --- | --- | --- |
| EN 12602 Prefabricated reinforced components of autoclaved aerated concrete | GERMANY: For the verification of the properties of the construction component design or testing are foreseen and standardized in the harmonized product standard; reference to the Eurocodes is not possible. When verifying by testing according to Annex B (indirectly referred to in Annex ZA) the necessary level of protection will not be attained (statistical analysis of the tests and determination of the characteristic values are missing). This Annex B will be excluded if necessary with the national transposition. For further comments on deficiencies see Construct 09/855. PG 208 states: "CEN/TC 177 agrees that some modifications according to the German comments could be made (see Resolution 124) in order to clarify the text." As far as the use of Annex B is concerned, deletion of this Annex has been proposed but meanwhile opposed by two delegations. FINLAND: Finland has the following technical reservations on EN 12602 based on the information given by Finnish experts: - In Clause 4.4 reference is made to EN 12269-2 which includes a test method for long term bond between reinforcement and AAC. Test according to this published test method are impossible to perform since testing room shall be kept on 50°C for one year. A new test method is under preparation in CEN/TC 177/WG3. It should be used for the CE-marking of these products. - In Clause A.4.1.3.2 calculation equiations (A.10) and (A.11) for shear capacity of AAC beams seem to be in some cases on unsafe side. This may cause serious safety problems. Calculations equations shall be improved. |  | Technical issue to be considered by the TC |
| prEN 13172 Conformity evaluation of thermal insulation products | FRANCE: The French Authorities would like to draw attention to the wording of prEN 13172:2007 concerning complaint procedures. If a product is non-compliant, a complaint is not generally lodged with the judicial authorities until attempts to settle a claim out of court have failed. The complaint procedure is a matter for the judicial authorities in application of the legislation and regulations in force, which take precedence over any contractual clauses, even if standardised and voluntarily agreed by all the contracting parties. As regards Annex F, which is described as being "informative", the penultimate paragraph of the foreword already states that: " .... Although the Annexes are informative in this standard, their use by the manufacturer will require that they assume a normative status. When an Annex is used the requirements in the Annex shall be followed, as given in the text." This could give the impression that manufacturers or users have no real protection and that application of the Standard does not give them any genuine rights. This undermines the credibility of the standards system and the French Authorities would like to see structural measures introduced with a view to preventing such situations from arising in future. | 2010-10-15 prEN 13172: Enquiry closed on 2010-09-01. The French comments are going to be considered in the draft going to FV. | Technical issue to be considered by the TC |
| EN 14023. Bitumen and bituminous binders. Framework specification for polymer modified bitumen | SPAIN Harmonized part of EN 14023 does not cover all the technical requirements given in the regulations of the Spanish Roads Administration (General Technical Prescriptions for Roads and Bridge Construction, in force since 1999, and more specifically in its article 215 “modified bitumen”. The missing requirements for modified bitumen to be included into harmonized part of EN 14023 are: − Fraas breaking point − Storage stability − Elastic recovery These requirements are already included in general part of EN 14023, referred in table 2 as additional requirements and characteristics that have been considered useful for specifications. Besides, there is the NOTE 1, which explains: Each country will then have a particular selection of specifications, which, if regulated, are covered in table 1 and which if commonly used by industry, are covered in table 2. It is useful for each country to publish in a national guidance document for each application, their requirements for polymer modified bitumen from table 1 and table2. The appropriate class for each technical requirement or application is selected in turn and the selection of classes should be made from past experience of successful use, on a regulation basis, in order to avoid unworkable combinations. In our opinion it is not only useful to include some of the characteristics in a national guidance but necessary to have them included in regulations, and therefore it is necessary to have them included in harmonized part and in the CE marking assessment. It is not possible with actual EN 14023 to comply with Technical Spanish regulations, published in 1999 and in force since then. In these regulations it is based the experience of successful use on a regional basis. Further more, in our opinion, compliance with clauses of Annex ZA, does not guarantee satisfaction of the essential requirements, specially concerning with durability of works. 2 We propose that the three characteristics mentioned above, are transferred from table 2 (framework specifications for additional requirements and classes of polymer modified bitumen) to table 1 (framework specifications for essential requirements and classes of polymer modified bitumens) and which it is more important, that these characteristics are included in the harmonized part of EN 14023 in table ZA.1: − Technical characteristic 1: Fraass breaking point represents low temperature behaviour, due to the same reasons argued by Finland in the case of paving grade bitumens: it is necessary to cover durability of bituminous mixtures in cold climate. Spain has several areas at high altitude, with cold temperatures in winter. In addition, Fraass breaking point is mandatory in the Spanish polymer modified bitumen specifications (1999). − Technical characteristic 2: Storage stability. Difference in softening point plus difference in penetration. These characteristics must be considered covered by the mandate due to the durability, together with resistance to hardening. Unlike paving grade bitumen, the polymer modified bitumen could include in their formulations products with physical and/or chemical incompatibilities with bitumen. Therefore the storage stability is an essential characteristic to guarantee that the characteristics declared by the supplier do not suffer significant changes during the storage period. Storage stability is also a mandatory characteristic in the Spanish polymer modified bitumen specifications (1999). − Technical characteristic 3: Elastic recovery (25ºC & 10ºC). Some typical applications of polymer modified bitumens require a significant capacity to recover from high strain. For this reason, in many national specifications, Spanish included, elastic recovery is considered as a mandatory characteristic. If this characteristic were not included in the essential characteristics of table 1, then some polymer modified bitumen (such as those formulated with plastomer polymers) could comply with the specification but not with the performances required by clients in the intended use. This characteristic is related with resistance and durability of works and it is necessary for the assessment of the essential requirements 1 or 4. | Message from ES authorities in 2011-02-02: In relation to the query on EN 13108-1 to 7 Bituminous mixtures, this group of standards begin now a revision process in which, the CEN/TC227/WG1 has shown interest on discussing and trying to solve the queries presented by Spain. In this situation, we hope that the comments will be included in the future works of the Technical Committee, so we should wait and follow the development of the new version of the EN 13108 package. | Technical issue to be considered by the TC |
| EN 15732 expanded-clay lightweight aggregates for lightweight fill and thermal insulation in civil engineering | FRANCE: Standard EN 15732 on expanded-clay lightweight aggregates for lightweight fill and thermal insulation in civil engineering has been established under CEN TC 88. The French Authorities wonder whether essential requirement No 3 on hygiene, health and the environment has genuinely been taken into account in this Standard, since in the body of the text a paragraph headed "dangerous substances" refers the reader to Annex ZA1, which refers back to the original paragraph. | 2010-10-15 Enquiry closed :2008-03-25 The French comments will be considered before the drafts goes to Formal Vote. | Technical issue to be considered by the TC |

GERMANY:     Deficiencies with regard to the reaction to fire behaviour of products

Although the following European product standards in the meantime makes reference to the European test and classification standards as e. g. EN 13501-1 they does not give details to the mounting and fixing of the products into the testing device. In case every test body determines the relevant provisions itself, comparable test results and comparable classifications are missing in Europe. For the time being, different reaction to fire classes might therefore be declared for a product depending on the test conditions having been chosen by the test body. This applies to the following harmonised standards:

EN 438-7 "Highpressure decorative laminates (HPL) - Sheets based on thermosetting resins (usually called laminates)"

EN 534 "Corrugated bitumen sheets"

EN 998-1 "Rendering and plastering mortar"

EN 1096-4 "Coated glass"

EN 1279-5 "Glass in building - Insulating glass units"

EN 1504-2 "Products and systems for the protection and repair of concrete structures"

EN 1504-3 "Products and systems for the protection and repair of concrete structures"

EN 1504-4 "Products and systems for the protection and repair of concrete structures"

EN 1873 "Prefabricated accessories for roofing - Individual roof lights of plastics"

EN 12859 "Gypsum blocks"

EN 13815 "Fibrous gypsum plaster casts"

EN 13830 "Curtain walling"

EN 13950 "Gypsum plasterboard thermal/acoustic insulation composite panels - Definitions, requirements and test methods"

EN 13964 "Suspended ceilings - Requirements and test methods"

EN 13986 "Wood-based panels for use in construction - Characteristics, evaluation of conformity and marking"

EN 14190 "Gypsum plasterboard products from reprocessing"

EN 14195 "Metal framing components for gypsum plasterboard systems"

EN 14246 "Gypsum elements for suspended ceilings"

EN 14449 "Glass in building - Laminated glass and laminated safety glass"

EN 14963 "Roof coverings - Continuous rooflights of plastics with or without upstands"

EN 15498 "Precast concrete products - Wood-chip concrete shuttering blocks - Product properties and performance"