COMMISSION IMPLEMENTING DECISION

of XXX

on the classification without further testing of certain uncoated wood floorings in accordance with EN14342 concerning their reaction to fire

THE EUROPEAN COMMISSION,

Having regard to the Treaty on the Functioning of the European Union,

Having regard to Council Directive 89/106/EEC of 21 December 1988, on the approximation of laws, regulations and administrative provisions of the Member States relating to construction products, and in particular Article 20(2) thereof,

Whereas:

- Council Directive 89/106/EEC envisages that in order to take account of different levels of protection for the construction works at national, regional or local levels, it may be necessary to establish in the interpretative documents classes corresponding to the performance of products in respect of each essential requirement. Those documents have been published as the “Communication of the Commission with regard to the interpretative documents of Directive 89/106/EEC.”

- With respect to the essential requirement of safety in the event of fire, interpretative document No 2 lists a number of interrelated measures which together define the fire safety strategy to be variously developed in the Member States.

- Interpretative document No 2 identifies one of those measures as the limitation of the generation and spread of fire and smoke within a given area by limiting the potential of construction products to contribute to the full development of a fire.

- The level of that limitation may be expressed only in terms of the different levels of reaction-to-fire performance of the products in their end-use application.

- By way of a harmonised solution, a system of classes was adopted in Commission Decision 2000/147/EC of 8 February 2000 implementing Council Directive 89/106/EEC as regard the classification of the reaction-to-fire performance of construction products.

- In the case of wood floorings in accordance with EN 14342 it is necessary to use the classification established in Decision 2000/147/EC.

- The reaction-to-fire performance of certain uncoated wood floorings, within the classification provided for in Decision 2000/147/EC, is well established and sufficiently well known to fire regulators in Member States that they do not require testing for this particular performance characteristic.

- The measures provided for in this Decision are in accordance with the opinion of the Standing Committee on Construction,

HAS ADOPTED THIS DECISION:

Article 1

The construction products and/or materials which satisfy all the requirements of the performance characteristic “reaction-to-fire” without need for further testing are set out in the Annex.

Article 2

The specific classes to be applied to different construction products and/or materials, within the reaction-to-fire classification adopted in Decision 2000/147/EC, are set out in the Annex to this Decision. Products shall be considered in relation to their end-use application, where relevant.

Article 3

This Decision shall enter into force on the first day following that of its publication in the Official Journal of the European Union.

Done at Brussels,

For the Commission

On behalf of the President 
	Antonio Tajani
	Vice President

ANNEX

The table set out in this Annex, lists construction products and/or materials which satisfy all of the requirements for the performance characteristic reaction to fire without need for testing.

TABLE: CLASSES OF REACTION TO FIRE PERFORMANCE FOR CERTAIN UNCOATED WOOD FLOORINGS IN ACORDANCE WITH EN 14342

(complementary to table 1 in Commission Decision 2006/213/EC)

| Product 1,7) | Product detail 4) | Minimum mean density 5) (kg/m³) | Minimum overall thickness (mm) | End use condition | Class for floorings 3) |
| --- | --- | --- | --- | --- | --- |
| Wood flooring | Solid wood flooring of pine or spruce | Pine: 480 Spruce: 400 | 14 | Without air gap underneath | Dfl-s1 |
| Wood flooring | Solid flooring of beech, oak, pine or spruce | Beech: 700 Oak: 700 Pine: 430 Spruce: 400 | 20 | With or without air gap underneath | Dfl-s1 |
| Wood parquet | Solid wood (one layer) parquet of walnut | 650 | 8 | Glued to substrate 6) | Dfl-s1 |
| Wood parquet | Solid (one layer) parquet of oak, maple or ash | Ash:650 Maple: 650 Oak: 720 | 8 | Glued to substrate 6) | Dfl-s1 |
| Wood parquet | Multilayer parquet with oak top layer, at least 3,5 mm | 550 | 15 2) | Without air gap underneath | Dfl-s1 |
| Wood flooring and parquet | Solid wood flooring and parquet not specified above | 400 | 6 | All | Efl |
| - Mounted in accordance with EN ISO 9239-1, on a substrate of at least Class D-s2, d0 with minimum density of 400 kg/m³ or with an air gap (minimum height 30 mm) underneath. - An interlayer of at least Class Efl and with maximum thickness 3 mm and minimum density of 280 kg/m3 may be included. - Class as provided for in Commission Decision 2000/147/EC Annex Table 2. - Without surface coatings. - Conditioned according to EN 13238 (50 % RH, 23 °C). - Substrate at least Class D-s2, d0. - Applies also to steps of stairs. |  |  |  |  |  |

OJ L 40, 11.2.1989, p12.

OJ C 62, 28.2.1994, p. 1

OJ L 50 23.2.2000, p. 14. Decision as amended by Decision 2003/632/EC (OJ L 220, 3.9.2003, p. 5).